## Appendix A.

.

Table A1. Characteristics of the samples from the Bayan qagan dongshan Sn-Pb-Zn-Ag deposit analyzed by EPMA and LA-ICP-MS.

| Sample No. | Location | Mineralization stages |  |  | Structures | Major mineral | Description |
| --- | --- | --- | --- | --- | --- | --- | --- |
| BY-B4 | Granite porphyry at 860 m level | Stage Ⅰ | – | – | Disseminated structure | Sphalerite | It is characterized by the disseminated sphalerite, tourmaline and a small amount of cassiterite, arsenopyrite and pyrite. |
| BY-B7 | Granite porphyry at 860 m level |  | – | – | Disseminated structure | Sphalerite | It is characterized by the disseminated sphalerite, tourmaline and a small amount of cassiterite, arsenopyrite and pyrite. |
| BY-B8 | III-1 orebody at 860 m level | Stage Ⅱ | Stage Ⅱ-1 | – | Breccia structure | Cassiterite + Sphalerite + Arsenopyrite + Pyrite | Sphalerite Ⅱ-1 mainly coexists with cassiterite and partially accompanies with pyrite and arsenopyrite. |
| BY-B9-1 | III-3 orebody at 860 m level |  | Stage Ⅱ-2 | Stage Ⅱ-2a | Massive structure + Vein structure | Sphalerite + Stannite + Galena + Pyrite | Sphalerite Ⅱ-2a is surrounded by stannite and locally contains galena veinlets. |
| BY-B19 | III-4 orebody at 860 m level |  |  | Stage Ⅱ-2b | Massive structure + Vein structure | Sphalerite + Stannite + Chalcopyrite + Galena | Sphalerite Ⅱ-2b is crowded with a small amount of micro inclusions of chalcopyrite, and locally crosscut by veinlets containing galena. |
| BY-B37 | III-5 orebody at 860 m level |  |  | Stage Ⅱ-2c | Massive structure + Vein structure | Sphalerite + Stannite + Chalcopyrite + Galena + Arsenopyrite | 1. Sphalerite Ⅱ-2c is typically characterized by the development of chalcopyrite inclusions, which is larger than that of sphalerite Ⅱ-2b. 2. Sphalerite Ⅱ-2c is partially cut by chalcopyrite veinlets and locally contains aggregates of fine-grained arsenopyrite. |

| Sample No. | Location | Mineralization stages |  |  | Structures | Major mineral | Description |
| --- | --- | --- | --- | --- | --- | --- | --- |
| BY-B9-2 | III-6 orebody at 900m level | Stage Ⅱ | Stage Ⅱ-3 | Stage Ⅱ-3a | Vein structure | Sphalerite+ Galena+ Pyrite+ Stannite+ Chalcostibite | Sphalerite Ⅱ-3a commonly appears as irregular intergranular aggregates and coexists with galena and minor amounts of stannite and chalcostibite. |
| BY-B29 | III-7 orebody at 900m level |  |  | Stage Ⅱ-3b | Vein structure | Sphalerite+Chalcostibite+Jameso-nite+Pyrite+ Stannite | Sphalerite Ⅱ-3b is intermingled with Sb-bearing minerals (e.g., tetrahedrite, chalcostibite, and Jamesonite ect.) and generally occurs as aggregates of fine-grained. |

Table A2. EPMA data of sphalerite from the Bayan qagan dongshan Sn-Pb-Zn-Ag deposit (data in wt%).

| Spot No. | Sphalerite subtype | Zn | As | Se | Ag | Cd | Bi | Sn | Fe | Cu | Mn | Ni | S | Te | Sb | Co | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BY-B4-1 | Sphalerite Ⅰ | 53.37 | 0.00 | 0.00 | 0.00 | 0.05 | 0.00 | 0.00 | 11.88 | 0.00 | 0.03 | 0.00 | 34.22 | 0.10 | 0.02 | 0.02 | 99.69 |
| BY-B4-2 | Sphalerite Ⅰ | 53.40 | 0.03 | 0.04 | 0.00 | 0.10 | 0.04 | 0.04 | 11.79 | 0.00 | 0.09 | 0.00 | 34.48 | 0.00 | 0.02 | 0.02 | 100.05 |
| BY-B4-3 | Sphalerite Ⅰ | 53.31 | 0.00 | 0.06 | 0.00 | 0.10 | 0.00 | 0.02 | 11.69 | 0.05 | 0.10 | 0.00 | 33.99 | 0.04 | 0.03 | 0.02 | 99.41 |
| BY-B4-4 | Sphalerite Ⅰ | 53.04 | 0.00 | 0.06 | 0.00 | 0.09 | 0.00 | 0.00 | 11.87 | 0.01 | 0.08 | 0.03 | 34.69 | 0.12 | 0.00 | 0.02 | 100.01 |
| BY-B4-5 | Sphalerite Ⅰ | 53.57 | 0.00 | 0.04 | 0.00 | 0.05 | 0.00 | 0.03 | 11.76 | 0.00 | 0.12 | 0.00 | 33.86 | 0.26 | 0.00 | 0.00 | 99.69 |
| BY-B4-6 | Sphalerite Ⅰ | 54.91 | 0.16 | 0.04 | 0.00 | 0.05 | 0.00 | 0.00 | 11.59 | 0.01 | 0.11 | 0.00 | 33.04 | 0.32 | 0.00 | 0.01 | 100.24 |
| BY-B4-7 | Sphalerite Ⅰ | 54.91 | 0.01 | 0.02 | 0.00 | 0.08 | 0.04 | 0.00 | 11.24 | 0.06 | 0.05 | 0.00 | 33.76 | 0.17 | 0.03 | 0.02 | 100.39 |
| BY-B4-8 | Sphalerite Ⅰ | 54.19 | 0.01 | 0.01 | 0.00 | 0.07 | 0.00 | 0.03 | 11.37 | 0.00 | 0.07 | 0.00 | 34.05 | 0.16 | 0.02 | 0.00 | 99.98 |
| BY-B7-1 | Sphalerite Ⅰ | 53.73 | 0.00 | 0.00 | 0.00 | 0.10 | 0.00 | 0.00 | 11.38 | 0.00 | 0.26 | 0.01 | 34.42 | 0.00 | 0.00 | 0.00 | 99.9 |
| BY-B8-1 | Sphalerite Ⅱ-1 | 53.88 | 0.00 | 0.00 | 0.00 | 0.13 | 0.00 | 0.29 | 8.02 | 4.40 | 0.06 | 0.00 | 34.73 | 0.07 | 0.00 | 0.03 | 101.61 |
| BY-B8-2 | Sphalerite Ⅱ-1 | 52.30 | 0.06 | 0.00 | 0.00 | 0.09 | 0.00 | 0.00 | 11.97 | 0.07 | 0.06 | 0.00 | 34.71 | 0.00 | 0.00 | 0.03 | 99.29 |
| BY-B8-3 | Sphalerite Ⅱ-1 | 52.78 | 0.05 | 0.00 | 0.00 | 0.06 | 0.00 | 0.00 | 12.08 | 0.08 | 0.02 | 0.00 | 34.46 | 0.31 | 0.00 | 0.02 | 99.86 |
| BY-B8-4 | Sphalerite Ⅱ-1 | 52.88 | 0.00 | 0.01 | 0.00 | 0.11 | 0.00 | 0.00 | 12.18 | 0.03 | 0.04 | 0.02 | 34.51 | 0.00 | 0.00 | 0.04 | 99.82 |
| BY-B8-5 | Sphalerite Ⅱ-1 | 52.80 | 0.07 | 0.00 | 0.00 | 0.16 | 0.00 | 0.00 | 12.15 | 0.01 | 0.04 | 0.00 | 33.40 | 0.00 | 0.00 | 0.02 | 98.65 |
| BY-B8-6 | Sphalerite Ⅱ-1 | 51.88 | 0.01 | 0.00 | 0.00 | 0.10 | 0.00 | 0.00 | 11.92 | 0.03 | 0.00 | 0.00 | 34.21 | 0.00 | 0.00 | 0.04 | 98.19 |
| BY-B9-1-2 | Sphalerite Ⅱ-2a | 58.60 | 0.01 | 0.00 | 0.00 | 0.09 | 0.02 | 0.04 | 6.91 | 0.12 | 0.06 | 0.00 | 33.86 | 0.09 | 0.00 | 0.00 | 99.8 |
| BY-B9-1-3 | Sphalerite Ⅱ-2a | 55.92 | 0.00 | 0.04 | 0.00 | 0.09 | 0.00 | 0.02 | 9.49 | 0.03 | 0.04 | 0.02 | 33.95 | 0.00 | 0.00 | 0.00 | 99.6 |
| BY-B9-1-4 | Sphalerite Ⅱ-2a | 54.27 | 0.00 | 0.00 | 0.00 | 0.11 | 0.00 | 0.00 | 7.98 | 3.33 | 0.03 | 0.00 | 34.32 | 0.00 | 0.00 | 0.03 | 100.07 |
| BY-B9-1-5 | Sphalerite Ⅱ-2a | 57.06 | 0.00 | 0.01 | 0.00 | 0.08 | 0.00 | 0.00 | 7.35 | 0.31 | 0.02 | 0.00 | 34.23 | 0.00 | 0.01 | 0.04 | 99.11 |
| BY-B9-1-6 | Sphalerite Ⅱ-2a | 59.19 | 0.00 | 0.00 | 0.00 | 0.08 | 0.00 | 0.02 | 6.17 | 0.10 | 0.03 | 0.02 | 33.63 | 0.00 | 0.00 | 0.02 | 99.26 |
| BY-B9-1-7 | Sphalerite Ⅱ-2a | 59.09 | 0.00 | 0.00 | 0.00 | 0.09 | 0.01 | 0.00 | 6.35 | 0.13 | 0.03 | 0.00 | 33.72 | 0.15 | 0.00 | 0.02 | 99.59 |
| BY-B9-1-8 | Sphalerite Ⅱ-2a | 55.30 | 0.04 | 0.05 | 0 | 0.11 | 0 | 0 | 9.69 | 0.04 | 0.02 | 0 | 34.01 | 0 | 0 | 0.03 | 99.29 |

| Spot No. | Sphalerite subtype | Zn | As | Se | Ag | Cd | Bi | Sn | Fe | Cu | Mn | Ni | S | Te | Sb | Co | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BY-B19-1 | Sphalerite Ⅱ-2b | 57.32 | 0.00 | 0.00 | 0.00 | 0.05 | 0.02 | 0.00 | 7.47 | 0.32 | 0.07 | 0.02 | 34.30 | 0.21 | 0.00 | 0.03 | 99.81 |
| BY-B19-2 | Sphalerite Ⅱ-2b | 56.59 | 0.00 | 0.00 | 0.00 | 0.10 | 0.00 | 0.00 | 7.83 | 0.25 | 0.07 | 0.00 | 34.65 | 0.03 | 0.00 | 0.02 | 99.54 |
| BY-B19-3 | Sphalerite Ⅱ-2b | 55.90 | 0.00 | 0.00 | 0.00 | 0.08 | 0.00 | 0.00 | 8.93 | 0.16 | 0.05 | 0.02 | 34.53 | 0.10 | 0.01 | 0.00 | 99.78 |
| BY-B19-4 | Sphalerite Ⅱ-2b | 59.53 | 0.00 | 0.00 | 0.00 | 0.06 | 0.02 | 0.17 | 3.46 | 2.34 | 0.02 | 0.00 | 33.69 | 0.23 | 0.00 | 0.00 | 99.52 |
| BY-B19-5 | Sphalerite Ⅱ-2b | 56.73 | 0.00 | 0.00 | 0.00 | 0.04 | 0.00 | 0.00 | 5.98 | 4.75 | 0.06 | 0.01 | 33.83 | 0.00 | 0.01 | 0.00 | 101.41 |
| BY-B19-6 | Sphalerite Ⅱ-2b | 55.02 | 0.02 | 0.00 | 0.00 | 0.11 | 0.00 | 0.00 | 9.27 | 0.06 | 0.03 | 0.02 | 34.64 | 0.14 | 0.00 | 0.03 | 99.34 |
| BY-B37-1 | Sphalerite Ⅱ-2c | 57.12 | 0.02 | 0.00 | 0.00 | 0.10 | 0.00 | 0.05 | 7.63 | 0.30 | 0.06 | 0.00 | 34.23 | 0.02 | 0.00 | 0.01 | 99.54 |
| BY-B37-2 | Sphalerite Ⅱ-2c | 58.50 | 0.00 | 0.02 | 0.00 | 0.05 | 0.00 | 0.05 | 7.06 | 0.09 | 0.03 | 0.00 | 34.10 | 0.00 | 0.00 | 0.00 | 99.9 |
| BY-B37-3 | Sphalerite Ⅱ-2c | 58.21 | 0.00 | 0.00 | 0.00 | 0.09 | 0.00 | 0.00 | 7.02 | 0.22 | 0.05 | 0.01 | 34.03 | 0.00 | 0.00 | 0.01 | 99.64 |
| BY-B37-4 | Sphalerite Ⅱ-2c | 58.82 | 0.00 | 0.00 | 0.00 | 0.08 | 0.03 | 0.03 | 6.79 | 0.20 | 0.07 | 0.01 | 32.59 | 0.38 | 0.01 | 0.00 | 99.01 |
| BY-B37-5 | Sphalerite Ⅱ-2c | 58.99 | 0.04 | 0.00 | 0.00 | 0.07 | 0.00 | 0.00 | 6.67 | 0.25 | 0.05 | 0.00 | 34.12 | 0.10 | 0.00 | 0.00 | 100.29 |
| BY-B37-6 | Sphalerite Ⅱ-2c | 59.80 | 0.04 | 0.00 | 0.00 | 0.10 | 0.00 | 0.01 | 4.65 | 1.15 | 0.07 | 0.00 | 33.63 | 0.00 | 0.01 | 0.00 | 99.46 |
| BY-B37-7 | Sphalerite Ⅱ-2c | 59.35 | 0.00 | 0.01 | 0.00 | 0.02 | 0.00 | 0.00 | 5.67 | 1.13 | 0.05 | 0.00 | 34.18 | 0.00 | 0.00 | 0.01 | 100.42 |
| BY-B37-8 | Sphalerite Ⅱ-2c | 58.30 | 0.00 | 0.00 | 0.00 | 0.05 | 0.02 | 0.00 | 6.48 | 0.40 | 0.02 | 0.00 | 34.18 | 0.00 | 0.01 | 0.01 | 99.47 |
| BY-B37-9 | Sphalerite Ⅱ-2c | 57.06 | 0.00 | 0.00 | 0.00 | 0.16 | 0.01 | 0.16 | 5.51 | 3.59 | 0.05 | 0.00 | 33.39 | 0.00 | 0.00 | 0.01 | 99.94 |
| BY-B9-2-1 | Sphalerite Ⅱ-3a | 65.37 | 0.00 | 0.03 | 0.00 | 0.03 | 0.00 | 0.00 | 0.03 | 0.96 | 0.00 | 0.00 | 33.60 | 0.00 | 0.95 | 0.00 | 100.97 |
| BY-B9-2-2 | Sphalerite Ⅱ-3a | 61.57 | 0.03 | 0.00 | 0.01 | 0.02 | 0.00 | 0.00 | 0.04 | 2.05 | 0.00 | 0.04 | 33.27 | 0.00 | 2.46 | 0.01 | 99.5 |
| BY-B9-2-3 | Sphalerite Ⅱ-3a | 62.49 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.18 | 1.94 | 0.03 | 0.00 | 33.21 | 0.00 | 2.64 | 0.01 | 100.5 |
| BY-B9-2-4 | Sphalerite Ⅱ-3a | 65.64 | 0.00 | 0.00 | 0.00 | 0.00 | 0.01 | 0.00 | 0.06 | 0.48 | 0.00 | 0.00 | 33.36 | 0.00 | 1.04 | 0.00 | 100.59 |
| BY-B9-2-5 | Sphalerite Ⅱ-3a | 64.77 | 0.00 | 0.02 | 0.00 | 0.00 | 0.00 | 0.00 | 0.07 | 0.41 | 0.00 | 0.00 | 33.61 | 0.00 | 0.76 | 0.00 | 99.64 |
| BY-B9-2-6 | Sphalerite Ⅱ-3a | 67.48 | 0.02 | 0.00 | 0.00 | 0.01 | 0.00 | 0.01 | 0.12 | 0.13 | 0.01 | 0.01 | 33.40 | 0.00 | 0.20 | 0.01 | 101.4 |
| BY-B9-2-7 | Sphalerite Ⅱ-3a | 66.26 | 0.00 | 0.01 | 0.00 | 0.04 | 0.00 | 0.01 | 0.04 | 0.07 | 0.00 | 0.00 | 33.35 | 0.00 | 0.36 | 0.00 | 100.14 |
| BY-B9-2-8 | Sphalerite Ⅱ-3a | 64.55 | 0.00 | 0.00 | 0.00 | 0.01 | 0.02 | 0.01 | 0.10 | 0.21 | 0.01 | 0.00 | 33.79 | 0.00 | 0.58 | 0.00 | 99.28 |

| Spot No. | Sphalerite subtype | Zn | As | Se | Ag | Cd | Bi | Sn | Fe | Cu | Mn | Ni | S | Te | Sb | Co | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BY-B9-2-9 | Sphalerite Ⅱ-3a | 64.69 | 0.00 | 0.00 | 0.00 | 0.03 | 0.00 | 0.02 | 0.00 | 1.15 | 0.01 | 0.01 | 33.49 | 0.00 | 1.07 | 0.00 | 100.48 |
| BY-B29-1 | Sphalerite Ⅱ-3b | 63.77 | 0.09 | 0.00 | 0.00 | 0.01 | 0.00 | 0.00 | 0.07 | 0.68 | 0.00 | 0.01 | 33.55 | 0.00 | 1.36 | 0.01 | 99.55 |
| BY-B29-2 | Sphalerite Ⅱ-3b | 65.30 | 0.00 | 0.00 | 0.00 | 0.01 | 0.06 | 0.00 | 0.06 | 0.09 | 0.02 | 0.04 | 32.98 | 0.00 | 0.95 | 0.01 | 99.52 |
| BY-B29-3 | Sphalerite Ⅱ-3b | 64.14 | 0.04 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.02 | 0.18 | 0.02 | 0.01 | 33.02 | 0.00 | 1.45 | 0.01 | 98.89 |
| BY-B29-4 | Sphalerite Ⅱ-3b | 64.27 | 0.06 | 0.00 | 0.00 | 0.05 | 0.00 | 0.00 | 0.07 | 0.28 | 0.00 | 0.00 | 33.73 | 0.00 | 1.58 | 0.00 | 100.04 |
| BY-B29-5 | Sphalerite Ⅱ-3b | 61.06 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.24 | 1.73 | 0.00 | 0.02 | 32.90 | 0.00 | 3.30 | 0.00 | 99.25 |
| BY-B29-6 | Sphalerite Ⅱ-3b | 62.33 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.13 | 1.06 | 0.02 | 0.01 | 33.22 | 0.00 | 2.27 | 0.00 | 99.04 |

Note: The value of ‘0.00′ means the content of element are approximately zero.

Table A3. LA-ICP-MS data of sphalerite from the Bayan qagan dongshan Sn-Pb-Zn-Ag deposit (data in ppm).

| Spot No. | Sphalerite subtype | 55Mn | 59Co | 65Cu | 71Ga | 72Ge | 107Ag | 111Cd | 115In | 118Sn | 121Sb | 82Se | 122Te | 208Pb | 209Bi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BY-B4-L_1 | Sphalerite Ⅰ | 1064.0 | 0.39 | 881.0 | 5.5 | 1.96 | 7.4 | 3328.0 | 104.8 | 3.2 | 0.1 | 106.70 | 0.7 | 0.6 | <0.01 |
| BY-B4-L_2 | Sphalerite Ⅰ | 1383.4 | 0.47 | 387.0 | 3.1 | 1.38 | 4.9 | 3254.0 | 120.1 | 2.9 | 0.2 | 152.84 | 0.6 | 0.8 | <0.00 |
| BY-B4-L_3 | Sphalerite Ⅰ | 1303.3 | 0.48 | 1142.0 | 5.1 | 1.63 | 14.3 | 3279.0 | 157.0 | 2.4 | <0.05 | 157.66 | 0.3 | 0.5 | 0.02 |
| BY-B4-L_4 | Sphalerite Ⅰ | 1601.9 | 0.44 | 2884.0 | 1.6 | 0.56 | 21.9 | 3337.0 | 30.2 | 14.4 | 0.2 | 26.01 | 2.8 | 1.1 | <0.00 |
| BY-B4-L_5 | Sphalerite Ⅰ | 1376.7 | 0.44 | 170.0 | 1.7 | <0.39 | 1.8 | 3441.0 | 59.2 | 3.8 | 0.2 | <9.36 | 0.7 | 0.6 | 0.02 |
| BY-B4-L_6 | Sphalerite Ⅰ | 1252.1 | 0.32 | 84.0 | 1.5 | <0.27 | 3.2 | 3281.0 | 75.8 | 2.5 | 0.6 | 23.70 | 0.6 | 1.8 | 0.02 |
| BY-B4-L_7 | Sphalerite Ⅰ | 896.4 | <0 | 1618.0 | 0.7 | 0.6 | 9.0 | 3312.0 | 58.3 | 3.2 | 0.8 | 26.18 | 0.7 | 0.4 | 0.01 |
| BY-B4-L_8 | Sphalerite Ⅰ | 1044.2 | 0.05 | 1618.0 | 9.1 | <0.26 | 12.0 | 3383.0 | 57.4 | 64.6 | 4.2 | <0.00 | 12.7 | 1.4 | <0.00 |
| BY-B7-L_1 | Sphalerite Ⅰ | 3021.5 | 3.46 | 469.0 | 0.5 | 0.13 | 7.4 | 4175.0 | 88.3 | 102.4 | 19.4 | 9.26 | 24.3 | 36.2 | 0.08 |
| BY-B8-L_1 | Sphalerite Ⅱ-1 | 466.1 | 25.2 | 956.6 | 2.3 | <0.30 | 3.0 | 6,423.8 | 1,216.7 | 148.9 | 18.8 | 12.09 | 28.1 | 0.3 | 0.2 |
| BY-B8-L_2 | Sphalerite Ⅱ-1 | 454.6 | 29.8 | 800.3 | 1.8 | <0.39 | 3.4 | 6,481.7 | 1,422.9 | 36.1 | 11.4 | 21.10 | 7.9 | 0.2 | <0.00 |
| BY-B8-L_3 | Sphalerite Ⅱ-1 | 454.4 | 28.5 | 669.0 | 1.8 | <0.32 | 2.2 | 6,777.1 | 1,253.3 | 4.6 | <0.08 | 12.00 | 0.9 | <0.00 | <0.00 |
| BY-B8-L_4 | Sphalerite Ⅱ-1 | 465.0 | 30.3 | 456.6 | 3.1 | <0.31 | 1.4 | 6,295.2 | 889.4 | 2.5 | <0.00 | 14.42 | 0.3 | 0.1 | 0.02 |
| BY-B8-L_5 | Sphalerite Ⅱ-1 | 397.4 | 29.0 | 9,580.9 | 2.9 | 0.6 | 27.4 | 6,281.2 | 1,075.7 | 326.7 | 195.8 | 25.79 | 68.3 | 3.4 | 0.1 |
| BY-B8-L_6 | Sphalerite Ⅱ-1 | 458.7 | 27.0 | 767.2 | 2.2 | <0.36 | 2.1 | 6,161.1 | 1,175.3 | 180.4 | 11.1 | <5.65 | 34.4 | 802.0 | 0.02 |
| BY-B9-1-L_2 | Sphalerite Ⅱ-2a | 221.4 | 0.0 | 1,515.2 | 11.8 | <0.21 | 5.2 | 4,595.2 | 1,450.7 | 849.0 | 22.7 | <2.40 | 157.7 | 21.6 | 0.03 |
| BY-B9-1-L_3 | Sphalerite Ⅱ-2a | 286.4 | 0.7 | 1,565.8 | 15.0 | 1.1 | 2.8 | 4,725.0 | 85.1 | 453.4 | 1.3 | <0.00 | 87.8 | 1.7 | <0.00 |
| BY-B9-1-L_4 | Sphalerite Ⅱ-2a | 236.8 | 0.0 | 3,666.8 | 13.8 | <0.00 | 11.3 | 4,812.3 | 1,142.2 | 3,075.6 | 33.7 | <6.24 | 485.9 | 5.4 | <0.00 |
| BY-B9-1-L_5 | Sphalerite Ⅱ-2a | 266.3 | 1.9 | 1,164.6 | 10.3 | 0.6 | 4.1 | 4,996.1 | 1,210.2 | 566.0 | 15.6 | <4.17 | 106.3 | 18.7 | <0.00 |
| BY-B9-1-L_6 | Sphalerite Ⅱ-2a | 204.1 | 0.1 | 4,735.8 | 14.8 | <0.00 | 9.2 | 4,780.4 | 1,020.4 | 5,141.2 | 20.3 | <1.31 | 761.1 | 6.9 | <0.00 |
| BY-B9-1-L_7 | Sphalerite Ⅱ-2a | 227.2 | 0.1 | 1,193.2 | 10.5 | <0.40 | 2.8 | 4,196.7 | 1,641.5 | 300.0 | 8.7 | <1.67 | 60.7 | 1.6 | 0.01 |
| BY-B9-1-L_8 | Sphalerite Ⅱ-2a | 237.6 | 0.0 | 13,077.2 | 12.3 | 0.1 | 40.5 | 4,245.2 | 611.3 | 1732.0 | 231.5 | <3.72 | 268.2 | 111.4 | 0.57 |
| BY-B19-L_1 | Sphalerite Ⅱ-2b | 379.9 | 2.0 | 18,027.0 | 2.6 | <0.12 | 23.2 | 4,561.6 | 745.8 | 1,165.1 | 82.8 | <6.04 | 231.2 | 16.3 | 1.7 |

| Spot No. | Sphalerite subtype | 55Mn | 59Co | 65Cu | 71Ga | 72Ge | 107Ag | 111Cd | 115In | 118Sn | 121Sb | 82Se | 122Te | 208Pb | 209Bi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BY-B19-L_2 | Sphalerite Ⅱ-2b | 546.1 | 1.0 | 16,762.5 | 2.1 | <0.19 | 10.0 | 5,053.0 | 1,138.6 | 3,922.7 | 42.2 | <6.22 | 599.0 | 2.6 | 0.6 |
| BY-B19-L_3 | Sphalerite Ⅱ-2b | 509.4 | 1.2 | 10,939.7 | 3.2 | <0.24 | 15.6 | 4,701.7 | 810.4 | 817.0 | 27.7 | 9.80 | 153.0 | 2.8 | 1.1 |
| BY-B19-L_4 | Sphalerite Ⅱ-2b | 415.8 | 1.2 | 21,867.5 | 2.9 | 0.7 | 29.2 | 3,930.1 | 913.5 | 9,186.5 | 192.8 | <6.96 | 1,808.9 | 10.6 | 2.7 |
| BY-B19-L_5 | Sphalerite Ⅱ-2b | 591.6 | 1.5 | 8,267.0 | 2.2 | <0.02 | 11.6 | 5,094.7 | 763.1 | 4.6 | 2.4 | 10.39 | 0.9 | 0.8 | 0.1 |
| BY-B19-L_6 | Sphalerite Ⅱ-2b | 407.4 | 0.1 | 10,553.0 | 8.2 | 0.0 | 14.9 | 4779.3 | 1441.1 | 828.8 | 67.2 | <3.95 | 142.5 | 11.1 | 1.30 |
| BY-B37-L_1 | Sphalerite Ⅱ-2c | 536.4 | 2.5 | 10,738.5 | 5.7 | <0.00 | 474.3 | 3,792.5 | 467.7 | 1,102.8 | 2,658.0 | <5.91 | 210.0 | 6,351.8 | 131.0 |
| BY-B37-L_2 | Sphalerite Ⅱ-2c | 559.3 | 3.1 | 9,517.5 | 11.0 | 0.6 | 174.9 | 3,500.2 | 388.2 | 4,717.4 | 1,678.3 | <4.70 | 748.8 | 917.6 | 42.9 |
| BY-B37-L_3 | Sphalerite Ⅱ-2c | 543.8 | 9.8 | 7,228.1 | 9.2 | <0.31 | 39.6 | 3,870.1 | 397.4 | 1,409.8 | 101.1 | <4.10 | 253.1 | 126.3 | 3.5 |
| BY-B37-L_4 | Sphalerite Ⅱ-2c | 533.8 | 8.1 | 11,182.3 | 9.9 | 0.7 | 1,682.3 | 4,400.5 | 216.8 | 340.9 | 7,006.0 | <8.24 | 70.1 | 3,732.5 | 468.5 |
| BY-B37-L_5 | Sphalerite Ⅱ-2c | 594.1 | 14.4 | 8,242.8 | 6.9 | <0.42 | 46.5 | 4,411.9 | 464.0 | 197.0 | 133.9 | <0.00 | 41.1 | 51.1 | 0.4 |
| BY-B37-L_6 | Sphalerite Ⅱ-2c | 412.0 | 2.0 | 16,162.3 | 8.0 | 2.3 | 360.2 | 2,978.0 | 535.1 | 5,213.9 | 1,785.1 | <0.00 | 810.4 | 222.3 | 16.7 |
| BY-B37-L_7 | Sphalerite Ⅱ-2c | 562.9 | 1.9 | 11,930.6 | 9.9 | <0.00 | 230.7 | 3,566.6 | 550.1 | 2,758.1 | 1,447.9 | <5.14 | 515.5 | 521.9 | 8.9 |
| BY-B37-L_8 | Sphalerite Ⅱ-2c | 451.2 | 12.8 | 20,781.8 | 9.0 | 3.7 | 57.6 | 4,368.8 | 477.5 | 1,664.5 | 73.4 | <5.68 | 303.6 | 36.9 | 0.8 |
| BY-B37-L_9 | Sphalerite Ⅱ-2c | 641.6 | 15.3 | 9,528.4 | 9.1 | 0.2 | 17.9 | 5442.3 | 370.2 | 163.4 | 411.2 | <5.96 | 38.1 | 64.4 | 10.07 |
| BY-B9-2-L_1 | Sphalerite Ⅱ-3a | 4.8 | 1.2 | 1,689.1 | 2.4 | 0.8 | 884.5 | 344.9 | 66.7 | 820.8 | 8,975.0 | 50.97 | 163.7 | 48,200.0 | 322.2 |
| BY-B9-2-L_2 | Sphalerite Ⅱ-3a | 0.5 | 5.7 | 4,701.8 | 6.1 | 0.7 | 544.6 | 330.6 | 43.9 | 976.5 | 6,174.4 | <6.89 | 197.2 | 8,283.2 | 47.4 |
| BY-B9-2-L_3 | Sphalerite Ⅱ-3a | 1.3 | 3.4 | 3,281.3 | 3.6 | 0.2 | 588.2 | 398.9 | 50.2 | 819.8 | 4,723.5 | 22.87 | 152.5 | 5,506.2 | 29.6 |
| BY-B9-2-L_4 | Sphalerite Ⅱ-3a | 1.1 | 0.7 | 883.1 | 2.7 | 0.5 | 631.3 | 440.4 | 67.2 | 1,076.4 | 4,658.0 | 21.48 | 201.2 | 36,148.6 | 201.4 |
| BY-B9-2-L_5 | Sphalerite Ⅱ-3a | 1.0 | 3.8 | 4,440.2 | 3.0 | 0.4 | 656.7 | 412.8 | 70.2 | 2,382.8 | 5,478.8 | 21.30 | 418.9 | 3,469.2 | 53.2 |
| BY-B9-2-L_6 | Sphalerite Ⅱ-3a | 7.4 | 5.3 | 5,298.9 | 1.2 | 0.3 | 1,014.6 | 377.1 | 53.0 | 902.6 | 13,727.1 | 23.58 | 170.7 | 52,379.3 | 123.7 |
| BY-B9-2-L_7 | Sphalerite Ⅱ-3a | 6.6 | 4.0 | 4,322.0 | 1.9 | 0.2 | 873.1 | 437.2 | 51.7 | 1,125.4 | 11,008.4 | 25.93 | 191.2 | 28,030.8 | 95.9 |
| BY-B9-2-L_8 | Sphalerite Ⅱ-3a | 0.5 | 0.6 | 45.2 | 1.7 | 0.1 | 203.5 | 498.2 | 34.9 | 589.3 | 2,721.4 | 11.45 | 114.7 | 1,618.9 | 1.6 |
| BY-B9-2-L_9 | Sphalerite Ⅱ-3a | 1.0 | 3.5 | 3,355.3 | 5.7 | 0.1 | 871.3 | 490.8 | 90.9 | 967.2 | 5601.6 | 34.25 | 158.2 | 80162.9 | 143.19 |

| Spot No. | Sphalerite subtype | 55Mn | 59Co | 65Cu | 71Ga | 72Ge | 107Ag | 111Cd | 115In | 118Sn | 121Sb | 82Se | 122Te | 208Pb | 209Bi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BY-B29-L_1 | Sphalerite Ⅱ-3b | 0.2 | 1.2 | 10,844.7 | 1.0 | 0.1 | 1,110.8 | 202.4 | 9.1 | 103.1 | 22,237.3 | <7.43 | 21.4 | 13,997.8 | 2,935.3 |
| BY-B29-L_2 | Sphalerite Ⅱ-3b | 1.5 | 0.9 | 9,389.6 | 0.7 | 0.4 | 955.9 | 313.5 | 23.3 | 375.5 | 22,190.4 | <3.59 | 80.5 | 39,790.9 | 3,541.1 |
| BY-B29-L_3 | Sphalerite Ⅱ-3b | 5.9 | 0.5 | 12,689.4 | 1.0 | 0.2 | 925.8 | 195.5 | 106.1 | 5,066.5 | 27,911.7 | <9.03 | 994.7 | 11,441.2 | 10,435.5 |
| BY-B29-L_4 | Sphalerite Ⅱ-3b | 0.6 | 0.6 | 9,636.5 | 0.5 | 0.4 | 770.4 | 383.1 | 26.4 | 2,262.6 | 21,572.5 | <1.05 | 418.1 | 13,633.7 | 1,951.3 |
| BY-B29-L_5 | Sphalerite Ⅱ-3b | 2.4 | 0.3 | 106.8 | 1.7 | 0.0 | 163.4 | 45.3 | 18.5 | 45.0 | 9948.0 | <5.82 | 9.9 | 4772.9 | 6.52 |
| BY-B29-L_6 | Sphalerite Ⅱ-3b | 0.7 | 0.5 | 1,961.7 | 0.1 | 0.4 | 47.1 | 1140.0 | 4.1 | 1241.0 | 8082.5 | 18.02 | 229.2 | 8786.8 | 8.99 |

Note: The data denoted with ‘<’ are below the minimum detection limits.

Table A4. LA-MC-ICP-MS in situ S isotope compositions of various sphalerite subtypes from the Bayan qagan dongshan Sn-Pb-Zn-Ag deposit.

| Analysis spot | Sphalerite subtype | δ34Sv-CDT(‰) | Error (2σ) |
| --- | --- | --- | --- |
| BY-B4-S1 | Sphalerite Ⅰ | −6.0 | 0.2 |
| BY-B4-S2 | Sphalerite Ⅰ | −5.8 | 0.3 |
| BY-B4-S3 | Sphalerite Ⅰ | −3.6 | 0.3 |
| BY-B8-S4 | Sphalerite Ⅱ-1 | −5.9 | 0.1 |
| BY-B8-S5 | Sphalerite Ⅱ-1 | −3.6 | 0.2 |
| BY-B8-S6 | Sphalerite Ⅱ-1 | −3.8 | 0.1 |
| BY-B9-S7 | Sphalerite Ⅱ-2a | −3.7 | 0.2 |
| BY-B9-S8 | Sphalerite Ⅱ-2a | −4.0 | 0.2 |
| BY-B9-S9 | Sphalerite Ⅱ-2a | −4.6 | 0.2 |
| BY-B19-S11 | Sphalerite Ⅱ-2b | −4.3 | 0.3 |
| BY-B19-S12 | Sphalerite Ⅱ-2b | −4.3 | 0.2 |
| BY-B19-S13 | Sphalerite Ⅱ-2b | −4.7 | 0.2 |
| BY-B37-S14 | Sphalerite Ⅱ-2c | −2.5 | 0.7 |
| BY-B37-S15 | Sphalerite Ⅱ-2c | −1.7 | 0.7 |
| BY-B37-S16 | Sphalerite Ⅱ-2c | −1.1 | 0.9 |
| BY-B9-S19 | Sphalerite Ⅱ-3a | −4.7 | 0.1 |
| BY-B9-S20 | Sphalerite Ⅱ-3a | −5.2 | 0.2 |
| BY-B9-S21 | Sphalerite Ⅱ-3a | −5.5 | 0.1 |
| BY-B29-S23 | Sphalerite Ⅱ-3b | −5.3 | 0.3 |
| BY-B29-S28 | Sphalerite Ⅱ-3b | −4.6 | 0.2 |
| BY-B29-S29 | Sphalerite Ⅱ-3b | −4.6 | 0.2 |