Supplemental Material 1 for

Genesis of the Maweishan Pb–Zn deposit, eastern China and controls on the distribution and formation of sphalerite-hosted critical metal (Cd, Ga, and In) mineralization

Yue Lia,b, Feng Yuana,b,*, Simon M. Jowittc, Taofa Zhoua,b, Guangxian Liud, Xunyu Hue, Xiaohui Li a,b

a. School of Resources and Environmental Engineering, Hefei University of Technology, Hefei 230009, China

b. Anhui Provincial Key Laboratory for Deep Exploration, Evaluation and Utilization of Strategic Mineral Resources, Hefei 230009, China

c. Ralph J. Roberts Center for Research in Economic Geology, Nevada Bureau of Mines and Geology, University of Nevada Reno. Reno, NV 89557-0178, USA

d. Jiangxi Provincial Key Laboratory of Genesis and Prospect for Strategic Minerals, East China University of Technology, Nanchang 330013, China

e. Zijin School of Geology and Mining, Fuzhou University, Fuzhou 350108, China

*Corresponding author: yf_hfut@163.com

This Supplemental Material includes:

Table S1. Analytical conditions for in-situ garnet U–Pb LA–ICP–MS analysis.

Text S1. Analytical methods used during this study.

Table S2. Electron microprobe (EPMA) data for garnet analyzed during this study (in wt.%).

Table S3. LA–ICP–MS data for garnet from the Maweishan deposit analyzed during this study (in ppm).

Table S4. The results of in-situ garnet U–Pb LA–ICP–MS dating of samples from the Maweishan deposit.

Table S5. LA–ICP–MS data for sphalerite from the Maweishan deposit analyzed during this study (in ppm).

Table S6. Sulfur isotopic data for samples from the Maweishan deposit.

Table S1. Analytical conditions for LA–ICP–MS measurements

| Laboratory & Sample Preparation |  |
| --- | --- |
| Laboratory name | Yanduzhongshi Geological Analysis Laboratories Ltd., Beijing, China |
| Sample type/mineral | Garnet, Apatite, Scheelite |
| Sample preparation | Polished thin sections |
| Laser ablation system |  |
| Make, Model & type | NWR193 Ar-F excimer laser |
| Ablation cell & volume | In-house built cell, volume ca. 25cm3 |
| Laser wavelength (nm) | 193 nm |
| Pulse width (ns) | 4 ns |
| Fluence (J.cm-2) | 3.0J/cm2 |
| Repetition rate (Hz) | 15 Hz |
| Ablation duration (secs) | 40 secs |
| Ablation pit depth / ablation rate | 12-20 μm |
| Spot diameter (μm) nominal/actual | 55 μm |
| Sampling mode / pattern | Static spot ablation |
| Carrier gas | 100% He in the cell, Ar make-up gas combined using a Y-piece 50% along the sample transport line to the torch. |
| Cell carrier gas flow (l/min) | 0.6 L/min |
| ICP-MS Instrument |  |
| Make, Model & type | Analytikjena, PlasmaQuant MS, quadrupole ICP–MS |
| Sample introduction | Ablation aerosol |
| RF power (W) | 1300 W |
| Make-up gas flow (l/min) | 1.05 L/min Ar |
| Detection system | quadrupole |
| Masses measured | 206Pb, 207Pb, 208Pb, 232Th, 235U, 238U |
| Integration time per peak/dwell times (ms); quadrupole settling time between mass jumps | 30 ms for 206Pb, 35 ms for 207Pb, 15 ms for 208Pb, 10 ms for 232Th, 15 ms for 235U, 20 ms for 238U |
| Total integration time per output datapoint (secs) | ~0.2 secs |
| Sensitivity | 0.2% U |
| Data Processing |  |
| Gas blank | 20 secs |
| Calibration strategy | see in the main manuscript |
| Reference Material info | see in the main manuscript |
| Data processing package used / Correction for LIEF | ICPMSDataCal and ZSkits. LIEF correction assumes reference material and samples behave identically. |
| Mass discrimination | Mass bias correction for all ratios normalized to calibration reference material. |
| Common-Pb correction, composition and uncertainty | None applied. Ages calculated from regressions used in Tera-Wasserburg plots. |
| Uncertainty level & propagation | Ages are quoted at 2σ absolute, propagation is by quadratic addition. |

Text S1. Analytical methods used during this study

S1.1 Electron Probe Microanalysis (EPMA)

Garnet compositions were determined by electron probe microanalysis (EPMA) employing a JOEL JXA 8230 electron microprobe equipped with wave and energy dispersive detectors and a backscattered electron detector at the School of Resources and Environmental Engineering, Hefei University of Technology, Hefei, China. This instrument was also used for BSE imaging. The EPMA undertaken during this study used an accelerating voltage of 15 kV, a beam current of 20 nA, an electron beam diameter of 3 μm, and a counting time of 20 s. Natural and synthetic minerals were used as standards and a standard ZAF program was employed for matrix corrections. The analytical precision of the concentrations of the majority of elements determined during this analysis is better than 1%.

S1.2 Garnet LA–ICP–MS analysis

Garnet laser ablation–inductively coupled plasma–mass spectrometry (LA–ICP–MS) trace element analysis and mapping was undertaken at the In-situ Mineral Geochemistry Lab, Ore Deposit and Exploration Centre (ODEC), Hefei University of Technology, Hefei, China, using an Agilent 7900 Quadrupole ICP–MS coupled to a Photon Machines Analyte HE 193-nm ArF Excimer LA system. Argon was used as a make-up gas and was mixed with the carrier gas via a T-connector before entering the ICP (Ning et al., 2017; Wang et al., 2017). Trace element analysis was performed using a uniform spot size diameter of 40 μm at 8 Hz with a laser energy of ~4 J/cm2 and an ablation period of 40 s after 20 s of gas blank measurement. Standard reference materials NIST 610 (external standard) and NIST 612 were analyzed between every 13 unknowns to correct the time-dependent sensitivity and mass discrimination. These NIST reference values taken from the GeoReM database (Jochum et al., 2005). Offline data processing was performed using the ICPMSDataCal software program (Liu et al., 2008).

LA–ICP–MS elemental maps was generated at ODEC, School of Resources and Environmental Engineering, Hefei University of Technology, Hefei, China, using a PhotonMachines Analyte HE LA system equipped with 193-nm ArF Excimer laser that was coupled to an Agilent 7900 Quadrupole ICP–MS (Ning et al., 2017). Ablation was performed in an atmosphere of ultrahigh purity He (0.9 L/min) that was mixed with Ar (0.87 L/min) immediately after the ablation cell via a T-connector before entering the ICP. High resolution profiling used a setup where the signal-smoothing device, which is used for routine analysis, was removed, providing an almost instantaneous response time. The ICP–MS system was optimized daily to maximize the sensitivity of isotopes within the mass range of interest while also keeping the production of molecular oxide species (i.e., 232Th16O/232Th) as low as possible (usually <0.3%). Elemental maps were created by ablating sets of parallel line rasters in a grid across the sample. All analyses used a beam size of 30 µm and a scan speed of 30 µm/s. These analyses also used a laser repetition setting of 10 Hz at a constant energy output of 50 mJ, resulting in an energy density of ~3 J/cm2 at the target. A 20 s background acquisition time was acquired at the start of scanning with a delay of 20 s after ablation added to allow for cell wash-out, gas stabilization, and computer processing. Data calibration used a NIST 610 standard that was analyzed at the start and end of each mapping run. Images were compiled and processed using the program LIMS (Wang et al., 2017) with the average background subtracted from each raster and for every element before the resulting rasters were compiled into a 2D image displaying combined background/drift corrected intensity for each element (Wang et al., 2017).

S1.3 In-situ U–Pb dating

U–Pb dating of garnet was undertaken on regular polished thin sections. In-situ U–Pb geochronology was undertaken using LA–ICP–MS at the Yanduzhongshi Geological Analysis Laboratories Limited, Beijing, China. All reference materials were analysed at the beginning of the session and after every 10 unknown spots using the same conditions as used on the samples and each analysis began with a 20 second blank gas measurement followed by a further 40 seconds of analysis time when the laser was switched on. A flow of He carrier gas at a rate of 0.6 L/min carried particles ablated by the laser out of the chamber to be mixed with Ar gas and then carried to the plasma torch. Off-line data processing was completed using the ICPMSDataCal software (Liu et al., 2008), and results are plotted in Tera–Wasserburg diagrams using Isoplot Version 4.15 (Ludwig, 2012). Uncertainty propagation and data reporting follow the community-based guidelines of Horstwood et al. (2016) and Roberts et al. (2020).

S1.4 Sulfide LA–ICP–MS analysis

Trace element analysis of sulfides was conducted by LA–ICP–MS at the In-situ Mineral Geochemistry Lab, Ore Deposit and Exploration Centre (ODEC), Hefei University of Technology, Hefei, China. The analyses were carried out on an Agilent 7900 Quadrupole ICP–MS coupled to a Photon Machines Analyte HE 193-nm ArF Excimer Laser Ablation system equipped. Argon was used as the make-up gas and mixed with the carrier gas via a T-connector before entering the ICP (Ning et al., 2017; Wang et al., 2017). As the high He (0.9L/min) and Ar (~0.9L/min) flow rate, the cleaning efficiency is really high, the signal increase to top less than 1s, and washout time is less than 1.5s. The element signals were not welly smoothed during ablation. Each analysis was performed by a uniform spot size diameter of 40 µm at 8 Hz with energy of ~2 J/cm2 for 40s after measuring the gas blank for 20s. Standard reference materials NIST 610, NIST 612, BCR-2G were used as external standards to generate a calibration curve. Concentration data for the NIST standards were taken from the GeoReM database (Jochum et al., 2005). Offline data processing was performed using the ICPMSDataCal software program (Liu et al., 2008).

S1.5 In-situ sulfur isotopic analysis

In-situ sulfur isotopic analysis was undertaken on sulfides using multicollector–inductively coupled plasma–mass spectrometry (MC–ICP–MS) utilizing a Nu Plasma II instrument coupled with a Resonetics–S155 excimer ArF laser ablation (LA) system at the State Key Laboratory of Geological Process and Mineral Resources (GPMR), China University of Geosciences, Wuhan, China. These analyses used a 33 m diameter laser beam with a frequency of 10 Hz and a 40 s ablation period, with ablated areas picked to avoid any small sulfide inclusions with different compositions to the hosting sulfides. Standard sample bracketing was used to determine the δ34S values of samples during MC–ICP–MS analysis with true sulfur isotopic ratios obtained by correcting for instrumental mass bias using linear interpolation between biases calculated from two neighboring standard analyses. Isotope ratio data are reported in delta notation (‰) relative to the V-CDT standard (Ding et al., 2001). The analytical precision of the in-situ S isotopic analysis undertaken during this study (1) is ± 0.1‰ and details of the analytical conditions and procedures used are given in Zhu et al. (2016, 2017). An in-house pyrite standard named WS-1 (natural pyrite crystal from the Wenshan polymetallic skarn deposit, Yunnan Province, China) is used to calibrate the mass bias for S isotopes (Zhu et al., 2016, 2017), and the δ34SV-CDT values (+1.1 ± 0.2‰) of WS-1 natural pyrite were determined with SIMS at the Chinese Academy of Geochemistry, Guangzhou (Zhu et al., 2016). The NBS-123 (δ34SV-CDT = +17.1 ± 0.2‰; Thornton et al., 2014) is used to calibrate the mass bias for sphalerite S isotopes.

References

Ding, T., Valkiers, S., Kipphardt, H., De Bievre, P., Taylor, P.D.P., Gonfiantini, R., and Krouse, R., 2001, Calibrated sulfur isotope abundance ratios of three IAEA sulfur isotope reference materials and V-CDT with a reassessment of the atomic weight of sulfur. Geochimica et Cosmochimica Acta: v. 65(15), p. 2433–2437.

Horstwood, M.S., Košler, J., Gehrels, G., Jackson, S.E., McLean, N.M., Paton, C., Pearson, N.J., Sircombe, K., Sylvester, P., Vermeesch, P., Bowring, J.F., Condon, D.J., Schoene, B., 2016. Community‐derived standards for LA‐ICP‐MS U‐(Th‐) Pb geochronology–Uncertainty propagation, age interpretation and data reporting. Geostandards and Geoanalytical Research, 40(3), 311-332.

Jochum, K.P., Nohl, U., Herwig, K., Lammel, E., Stoll, B., and Hofmann, A.W., 2005, GeoReM: a new geochemical database for reference materials and isotopic standards: Geostandards and Geoanalytical Research, v. 29(3), p. 333–338.

Liu, Y.S., Hu, Z.C., Gao, S., Günther, D., Xu, J., Gao, C.G., and Chen, H., 2008, In situ analysis of major and trace elements of anhydrous minerals by LA-ICP-MS without applying an internal standard: Chemical Geology, v. 257(1-2), p. 34–43.

Ning, S.Y., Wang, F.Y., Xue, W.D., and Zhou, T.F., 2017, Geochemistry of the Baoshan pluton in the Tongling region of the Lower Yangtze River Belt: Geochimica, v. 46, p. 397–412 (in Chinese with English abstract).

Roberts, N.M., Drost, K., Horstwood, M.S., Condon, D.J., Chew, D., Drake, H., Milodowski, A.E., McLean, N.M., Smye, A.J., Walker, R.J., Haslam, R., Hodson, K., Imber, J., Beaudoin, N., Lee, J.K., 2020. Laser ablation inductively coupled plasma mass spectrometry (LA-ICP-MS) U–Pb carbonate geochronology: strategies, progress, and limitations. Geochronology, 2, 33–61.

Thornton, S.F., Baker, K.M., Bottrell, S.H., Rolfe, S.A., McNamee, P., Forrest, F., Duffield, P., Wilson, R.D., Fairburn, A.W., Cieslak, L.A., 2014. Enhancement of in situ biodegradation of organic compounds in groundwater by targeted pump and treat intervention. Applied geochemistry, 48, 28-40.

Wang, F.Y., Ge, C., Ning, S.Y., Nie, L.Q., Zhong, G.X., and White, N.C., 2017, A new approach to LA–ICP–MS mapping and application in geology: Acta Petrologica Sinica, v. 33(11), p. 3422–3436 (in Chinese with English abstract).

Zhu, Z.Y., Cook, N.J., Yang, T., Ciobanu, C.L., Zhao, K.D., and Jiang, S.Y., 2016, Mapping of sulfur isotopes and trace elements in sulfides by LA–(MC)–ICP–MS: potential analytical problems, improvements and implications: Minerals, v. 6(4), article 110.

Zhu, Z.Y., Jiang, S.Y., Ciobanu, C.L., Yang, T., and Cook, N.J., 2017, Sulfur isotope fractionation in pyrite during laser ablation: Implications for laser ablation multiple collector inductively coupled plasma mass spectrometry mapping: Chemical Geology, v. 450, p. 223–234.

Table S2. Electron microprobe (EPMA) data for garnet analyzed during this study (in wt.%).

| Spot number | SiO2 | TiO2 | Al2O3 | FeO | MnO | MgO | CaO | Na2O | K2O | Cr2O3 | NiO | Total | Grossular | Andradite | Spessartine+ Pyrope+Almandine |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MWS-Grt-1-01 | 37.33 | 0.05 | 9.02 | 17.92 | 0.81 | 0.02 | 33.78 | 0.02 | 0.00 | 0.02 | 0.00 | 98.87 | 38.72 | 57.85 | 3.43 |
| MWS-Grt-1-02 | 37.50 | 0.00 | 8.29 | 18.70 | 0.84 | 0.02 | 33.53 | 0.01 | 0.00 | 0.05 | 0.03 | 98.97 | 35.75 | 60.60 | 3.65 |
| MWS-Grt-1-03 | 37.40 | 0.04 | 8.67 | 18.90 | 0.84 | 0.04 | 33.44 | 0.01 | 0.00 | 0.00 | 0.00 | 99.33 | 35.92 | 59.53 | 4.55 |
| MWS-Grt-1-04 | 37.26 | 0.00 | 11.13 | 15.24 | 0.60 | 0.03 | 35.06 | 0.00 | 0.00 | 0.01 | 0.00 | 99.34 | 48.07 | 50.38 | 1.55 |
| MWS-Grt-1-05 | 37.67 | 0.02 | 12.29 | 13.72 | 0.72 | 0.05 | 34.47 | 0.01 | 0.00 | 0.00 | 0.03 | 98.98 | 53.39 | 43.70 | 2.91 |
| MWS-Grt-1-06 | 37.75 | 0.11 | 12.78 | 12.51 | 0.82 | 0.08 | 34.46 | 0.00 | 0.00 | 0.00 | 0.00 | 98.51 | 56.56 | 40.79 | 2.66 |
| MWS-Grt-1-07 | 37.50 | 0.00 | 10.44 | 16.28 | 0.94 | 0.04 | 33.63 | 0.03 | 0.00 | 0.03 | 0.00 | 98.88 | 44.41 | 51.33 | 4.25 |
| MWS-Grt-1-08 | 37.87 | 0.04 | 10.24 | 16.26 | 0.77 | 0.03 | 34.05 | 0.00 | 0.00 | 0.00 | 0.00 | 99.26 | 44.71 | 51.93 | 3.36 |
| MWS-Grt-1-09 | 37.53 | 0.05 | 13.38 | 12.20 | 0.90 | 0.05 | 35.06 | 0.00 | 0.00 | 0.05 | 0.00 | 99.22 | 57.62 | 40.19 | 2.20 |
| MWS-Grt-1-10 | 38.16 | 0.07 | 13.14 | 12.14 | 0.83 | 0.07 | 34.42 | 0.03 | 0.00 | 0.00 | 0.00 | 98.85 | 58.21 | 38.78 | 3.01 |
| MWS-Grt-1-11 | 37.98 | 0.05 | 12.08 | 13.68 | 0.77 | 0.06 | 34.55 | 0.02 | 0.00 | 0.04 | 0.00 | 99.24 | 53.28 | 44.04 | 2.68 |
| MWS-Grt-1-12 | 38.11 | 0.12 | 12.27 | 12.84 | 0.66 | 0.10 | 34.56 | 0.01 | 0.00 | 0.01 | 0.00 | 98.68 | 55.46 | 42.38 | 2.16 |
| MWS-Grt-1-13 | 38.19 | 0.06 | 13.10 | 12.14 | 0.76 | 0.07 | 34.59 | 0.03 | 0.00 | 0.00 | 0.03 | 98.96 | 58.29 | 39.06 | 2.64 |
| MWS-Grt-1-14 | 36.61 | 0.00 | 10.98 | 16.67 | 1.04 | 0.04 | 33.77 | 0.01 | 0.00 | 0.00 | 0.04 | 99.17 | 43.08 | 52.09 | 4.83 |
| MWS-Grt-2-01 | 34.33 | 0.00 | 0.00 | 29.77 | 0.34 | 0.04 | 32.39 | 0.03 | 0.00 | 0.00 | 0.03 | 96.92 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-02 | 34.43 | 0.00 | 0.00 | 29.70 | 0.34 | 0.04 | 32.16 | 0.00 | 0.00 | 0.01 | 0.01 | 96.70 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-03 | 34.33 | 0.00 | 0.02 | 29.83 | 0.34 | 0.06 | 32.16 | 0.02 | 0.00 | 0.00 | 0.02 | 96.76 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-04 | 34.43 | 0.00 | 0.00 | 29.87 | 0.31 | 0.06 | 32.27 | 0.00 | 0.00 | 0.03 | 0.04 | 97.02 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-05 | 34.10 | 0.00 | 0.05 | 30.34 | 0.44 | 0.05 | 31.92 | 0.00 | 0.00 | 0.03 | 0.01 | 96.96 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-06 | 34.21 | 0.02 | 0.06 | 29.87 | 0.47 | 0.04 | 31.90 | 0.01 | 0.00 | 0.00 | 0.00 | 96.57 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-07 | 33.91 | 0.00 | 0.17 | 29.71 | 0.47 | 0.05 | 31.98 | 0.00 | 0.00 | 0.00 | 0.00 | 96.29 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-08 | 34.02 | 0.03 | 0.10 | 30.02 | 0.46 | 0.05 | 31.90 | 0.00 | 0.00 | 0.00 | 0.00 | 96.57 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-09 | 34.31 | 0.01 | 0.23 | 30.04 | 0.38 | 0.04 | 32.33 | 0.00 | 0.00 | 0.01 | 0.02 | 97.36 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-10 | 34.24 | 0.00 | 0.28 | 30.19 | 0.35 | 0.05 | 32.32 | 0.00 | 0.00 | 0.00 | 0.03 | 97.46 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-11 | 34.39 | 0.06 | 0.23 | 29.79 | 0.33 | 0.02 | 32.01 | 0.00 | 0.00 | 0.00 | 0.02 | 96.85 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-12 | 34.24 | 0.00 | 0.23 | 29.81 | 0.36 | 0.01 | 31.83 | 0.00 | 0.00 | 0.00 | 0.00 | 96.48 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-13 | 34.22 | 0.01 | 0.11 | 30.19 | 0.41 | 0.02 | 31.58 | 0.00 | 0.00 | 0.01 | 0.00 | 96.56 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-14 | 34.17 | 0.00 | 0.07 | 29.84 | 0.35 | 0.02 | 32.28 | 0.01 | 0.00 | 0.00 | 0.00 | 96.74 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-15 | 34.24 | 0.03 | 0.17 | 29.80 | 0.36 | 0.05 | 31.98 | 0.00 | 0.00 | 0.00 | 0.00 | 96.62 | 0.00 | 100.00 | 0.00 |
| MWS-Grt-2-16 | 34.71 | 0.00 | 0.18 | 29.84 | 0.31 | 0.04 | 32.10 | 0.02 | 0.00 | 0.00 | 0.00 | 97.20 | 0.00 | 100.00 | 0.00 |

Table S3. LA–ICP–MS data for garnet from the Maweishan deposit analyzed during this study (in ppm, BDL = Below the Detection Limit).

| Spot number | Sc | Ti | V | Cr | Mn | Co | Ni | Cu | Zn | Ga | Y | Zr | La | Ce | Pr | Nd |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Detection limit | 0.30 | 4.75 | 0.35 | 3.17 | 3.77 | 0.35 | 1.81 | 0.64 | 3.17 | 0.46 | 0.15 | 0.31 | 0.12 | 0.12 | 0.09 | 0.55 |
| MWS-Grt-1-01 | 9.71 | 2047 | 14.5 | BDL | 6080 | BDL | BDL | BDL | BDL | 35.4 | 9.62 | 32.6 | 0.27 | 5.94 | 2.97 | 28.9 |
| MWS-Grt-1-02 | 15.47 | 6021 | 115 | BDL | 5647 | BDL | BDL | BDL | 5.47 | 27.9 | 12.7 | 166.6 | 0.12 | 2.70 | 1.32 | 14.5 |
| MWS-Grt-1-03 | 9.94 | 3426 | 140 | BDL | 5840 | 0.37 | 2.99 | BDL | 3.83 | 28.7 | 17.4 | 99.1 | 0.12 | 2.18 | 1.26 | 13.7 |
| MWS-Grt-1-04 | 15.51 | 3585 | 382 | 6.67 | 5598 | BDL | BDL | BDL | 3.63 | 43.1 | 51.1 | 89.1 | 0.13 | 2.16 | 1.05 | 11.0 |
| MWS-Grt-1-05 | 11.80 | 4579 | 32.3 | 27.2 | 7665 | 0.35 | 2.01 | BDL | 4.52 | 33.3 | 7.97 | 71.3 | 0.12 | 1.51 | 0.71 | 6.70 |
| MWS-Grt-1-06 | 8.72 | 1352 | 41.9 | BDL | 6515 | BDL | BDL | BDL | BDL | 38.8 | 8.37 | 82.5 | 0.12 | 1.81 | 0.90 | 7.67 |
| MWS-Grt-1-07 | 8.11 | 1119 | 26.7 | BDL | 6309 | BDL | BDL | BDL | BDL | 25.0 | 6.47 | 79.5 | 0.15 | 2.90 | 1.41 | 11.8 |
| MWS-Grt-1-08 | 7.71 | 789 | 36.2 | BDL | 6334 | BDL | 2.07 | BDL | BDL | 39.3 | 7.45 | 45.8 | 0.17 | 2.43 | 1.17 | 11.4 |
| MWS-Grt-1-09 | 2.09 | 1081 | 37.7 | BDL | 7274 | BDL | BDL | BDL | BDL | 41.0 | 6.29 | 75.7 | 0.18 | 2.17 | 0.96 | 9.09 |
| MWS-Grt-1-10 | 2.57 | 1356 | 34.1 | 3.48 | 4773 | BDL | BDL | BDL | 3.44 | 22.7 | 6.68 | 81.0 | 1.30 | 16.0 | 4.99 | 26.5 |
| MWS-Grt-1-11 | 1.03 | 767 | 32.2 | BDL | 6526 | BDL | BDL | BDL | BDL | 23.0 | 5.43 | 44.0 | 0.34 | 3.37 | 1.55 | 11.5 |
| MWS-Grt-1-12 | 1.46 | 1368 | 30.1 | BDL | 5937 | BDL | BDL | BDL | BDL | 27.9 | 13.1 | 58.5 | 0.90 | 13.9 | 4.51 | 26.3 |
| MWS-Grt-1-13 | 0.88 | 427 | 19.1 | BDL | 5338 | BDL | BDL | BDL | BDL | 26.0 | 4.95 | 21.2 | 1.55 | 21.4 | 6.49 | 34.6 |
| MWS-Grt-1-14 | 4.25 | 2324 | 63.9 | 13.2 | 5165 | 0.62 | BDL | BDL | 5.34 | 26.3 | 9.16 | 114.5 | 0.38 | 2.43 | 0.97 | 9.79 |
| MWS-Grt-1-15 | 2.75 | 2437 | 43.7 | 6.78 | 5245 | 0.85 | BDL | BDL | 19.1 | 18.8 | 10.0 | 149.2 | 0.48 | 5.49 | 1.74 | 13.2 |
| MWS-Grt-1-16 | 2.11 | 1610 | 31.7 | BDL | 7387 | BDL | BDL | BDL | 3.42 | 29.8 | 8.04 | 123.9 | 0.10 | 2.01 | 0.75 | 8.10 |
| MWS-Grt-1-17 | 2.11 | 1722 | 30.3 | BDL | 7730 | BDL | BDL | BDL | 3.53 | 34.7 | 8.04 | 113.5 | 0.12 | 1.53 | 0.80 | 6.92 |
| MWS-Grt-1-18 | 2.07 | 1378 | 32.4 | 4.08 | 7595 | 0.40 | BDL | BDL | 3.55 | 40.7 | 8.09 | 106.0 | 0.10 | 1.59 | 0.75 | 7.87 |
| MWS-Grt-1-19 | 2.23 | 2842 | 74.6 | BDL | 6566 | BDL | BDL | BDL | 4.75 | 23.1 | 7.48 | 76.7 | 0.16 | 2.79 | 1.27 | 15.3 |
| MWS-Grt-1-20 | 6.39 | 5263 | 111 | 5.40 | 6380 | 0.61 | 2.04 | BDL | 5.41 | 26.7 | 9.72 | 122.2 | 0.18 | 2.44 | 1.10 | 13.8 |
| MWS-Grt-2-01 | 0.47 | BDL | 7.68 | BDL | 2331 | BDL | BDL | BDL | BDL | 27.6 | 1.27 | BDL | 2.08 | 2.98 | 0.33 | 1.49 |
| MWS-Grt-2-02 | 0.46 | BDL | 9.59 | BDL | 2439 | BDL | BDL | BDL | BDL | 20.6 | 0.50 | BDL | 1.40 | 2.43 | 0.38 | 1.44 |
| MWS-Grt-2-03 | 0.52 | BDL | 8.52 | BDL | 2314 | BDL | BDL | BDL | BDL | 27.5 | 2.03 | 0.45 | 1.59 | 2.68 | 0.32 | 1.54 |
| MWS-Grt-2-04 | 0.43 | BDL | 9.83 | BDL | 2887 | BDL | BDL | BDL | BDL | 26.2 | 0.79 | 0.48 | 2.49 | 4.33 | 0.39 | 1.57 |
| MWS-Grt-2-05 | 0.49 | BDL | 10.8 | BDL | 2808 | BDL | BDL | BDL | BDL | 28.6 | 0.77 | 0.38 | 3.16 | 5.55 | 0.54 | 2.00 |
| MWS-Grt-2-06 | 0.70 | BDL | 13.0 | BDL | 2642 | BDL | BDL | BDL | BDL | 21.5 | 1.59 | BDL | 2.88 | 3.59 | 0.43 | 1.98 |
| MWS-Grt-2-07 | 0.42 | BDL | 12.8 | BDL | 2620 | BDL | BDL | BDL | BDL | 21.9 | 1.19 | BDL | 3.35 | 3.97 | 0.38 | 2.05 |
| MWS-Grt-2-08 | 0.53 | 6.00 | 19.4 | 3.90 | 2920 | BDL | BDL | BDL | BDL | 26.6 | 3.15 | 0.87 | 1.94 | 4.17 | 0.48 | 2.19 |
| MWS-Grt-2-09 | 0.62 | BDL | 11.7 | 4.52 | 2909 | BDL | BDL | BDL | BDL | 27.5 | 0.58 | BDL | 2.70 | 3.86 | 0.34 | 1.51 |
| MWS-Grt-2-10 | 0.46 | BDL | 11.8 | BDL | 2685 | BDL | BDL | BDL | BDL | 59.0 | 0.30 | BDL | 1.84 | 3.59 | 0.22 | 0.99 |
| MWS-Grt-2-11 | 0.48 | BDL | 14.4 | 4.01 | 2691 | BDL | BDL | BDL | BDL | 54.3 | 0.34 | BDL | 2.70 | 4.40 | 0.27 | 0.78 |
| MWS-Grt-2-12 | 0.41 | BDL | 4.00 | BDL | 2731 | BDL | BDL | BDL | BDL | 64.8 | 1.12 | 0.43 | 2.33 | 3.07 | 0.21 | 0.66 |
| MWS-Grt-2-13 | 6.91 | BDL | 6.98 | BDL | 2923 | BDL | 2.93 | BDL | BDL | 47.3 | 1.02 | BDL | 2.93 | 4.16 | 0.20 | 0.59 |
| MWS-Grt-2-14 | 6.04 | 13.4 | 2.73 | BDL | 2990 | BDL | BDL | BDL | BDL | 50.2 | 1.38 | 0.94 | 2.82 | 3.26 | 0.17 | 0.55 |
| MWS-Grt-2-15 | 6.02 | BDL | 9.81 | BDL | 2812 | BDL | BDL | BDL | BDL | 23.9 | 0.63 | BDL | 0.91 | 1.17 | 0.13 | BDL |
| MWS-Grt-2-16 | 6.27 | 7.41 | 14.0 | BDL | 2737 | BDL | 1.90 | BDL | BDL | 24.0 | 0.90 | 0.32 | 2.39 | 1.87 | 0.13 | BDL |
| SRM 610 Reference values | 455 | 452 | 450 | 408 | 444 | 410 | 459 | 441 | 460 | 433 | 462 | 448 | 440 | 453 | 448 | 430 |
| SRM 610-1 | 470 | 462 | 453 | 446 | 469 | 449 | 518 | 494 | 440 | 463 | 490 | 471 | 474 | 475 | 482 | 486 |
| SRM 610-2 | 477 | 474 | 460 | 435 | 468 | 429 | 501 | 464 | 439 | 456 | 497 | 479 | 477 | 479 | 480 | 487 |
| SRM 610-3 | 481 | 482 | 451 | 419 | 444 | 412 | 470 | 436 | 434 | 433 | 489 | 469 | 464 | 462 | 463 | 456 |
| SRM 610-4 | 484 | 480 | 461 | 411 | 448 | 415 | 475 | 444 | 441 | 443 | 489 | 473 | 461 | 463 | 459 | 455 |
| SRM 610-5 | 481 | 473 | 452 | 409 | 440 | 406 | 453 | 429 | 430 | 437 | 490 | 467 | 459 | 462 | 459 | 460 |
| SRM 610-6 | 482 | 478 | 466 | 416 | 450 | 411 | 468 | 440 | 449 | 442 | 497 | 476 | 461 | 466 | 462 | 460 |
| SRM 612 Reference values | 39.9 | 44.0 | 38.8 | 36.4 | 38.7 | 35.5 | 38.8 | 37.8 | 39.1 | 36.9 | 38.3 | 37.9 | 36.0 | 38.4 | 37.9 | 35.5 |
| SRM 612-1 | 38.3 | 36.5 | 38.0 | 38.1 | 40.2 | 36.6 | 41.6 | 45.1 | 36.1 | 37.7 | 39.1 | 38.7 | 37.0 | 39.5 | 39.9 | 38.1 |
| SRM 612-2 | 38.3 | 42.0 | 39.2 | 27.0 | 38.4 | 37.6 | 39.7 | 42.0 | 36.0 | 38.5 | 37.5 | 38.3 | 37.3 | 39.2 | 38.6 | 35.7 |
| SRM 612-3 | 39.1 | 33.8 | 38.9 | 41.6 | 38.9 | 35.8 | 30.5 | 40.1 | 37.1 | 37.4 | 39.0 | 36.3 | 38.0 | 39.0 | 39.6 | 34.2 |
| SRM 612-4 | 38.3 | 33.9 | 39.3 | 34.6 | 37.7 | 35.2 | 37.3 | 42.8 | 33.8 | 37.7 | 37.5 | 38.7 | 36.8 | 39.7 | 38.8 | 37.6 |
| SRM 612-5 | 39.1 | 33.5 | 39.0 | 36.5 | 39.3 | 33.8 | 30.0 | 37.4 | 34.2 | 35.8 | 38.7 | 37.1 | 35.7 | 38.9 | 37.0 | 33.6 |
| SRM 612-6 | 38.8 | 31.5 | 38.6 | 34.3 | 39.2 | 34.6 | 32.3 | 37.9 | 31.9 | 36.2 | 37.7 | 38.4 | 35.0 | 40.1 | 37.8 | 35.7 |
| BCR-2G Reference values | 33.0 | 14100 | 425 | 17 | 1550 | 38.0 | 13.0 | 21.0 | 125 | 23.0 | 35.0 | 184 | 24.7 | 53.3 | 6.70 | 28.9 |
| BCR-2G-1 | 30.3 | 13250 | 427 | 14.4 | 1559 | 39.8 | 9.1 | 17.2 | 155 | 24.5 | 30.4 | 161 | 24.2 | 52.5 | 6.07 | 26.9 |
| BCR-2G-2 | 30.5 | 13600 | 431 | 14.8 | 1544 | 40.0 | 7.2 | 14.1 | 147 | 21.6 | 28.2 | 155 | 22.9 | 49.5 | 5.87 | 24.5 |
| BCR-2G-3 | 30.5 | 13666 | 438 | 16.8 | 1523 | 38.5 | 14.3 | 17.2 | 157 | 23.0 | 28.6 | 158 | 23.2 | 51.4 | 6.10 | 24.2 |
| BCR-2G-4 | 29.6 | 13711 | 438 | 15.3 | 1531 | 37.7 | 7.1 | 15.7 | 151 | 23.3 | 29.6 | 159 | 23.0 | 50.1 | 5.76 | 24.2 |
| BCR-2G-5 | 30.1 | 13738 | 436 | 14.4 | 1517 | 39.1 | 6.1 | 15.3 | 146 | 21.7 | 28.5 | 157 | 22.6 | 50.0 | 5.83 | 24.9 |
| BCR-2G-6 | 29.8 | 13766 | 434 | 16.5 | 1500 | 37.3 | 11.0 | 16.0 | 150 | 21.7 | 27.6 | 155 | 21.9 | 48.6 | 6.01 | 24.1 |

Continued TABLE S3.

| Spot number | Sm | Eu | Gd | Tb | Dy | Ho | Er | Tm | Yb | Lu | W | Th | U |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Detection limit | 0.63 | 0.17 | 0.58 | 0.08 | 0.35 | 0.08 | 0.26 | 0.08 | 0.37 | 0.08 | 0.33 | 0.08 | 0.06 |
| MWS-Grt-1-01 | 11.35 | 1.37 | 6.75 | 0.54 | 2.02 | 0.24 | 0.53 | 0.07 | 0.49 | 0.08 | 2.03 | 0.59 | 6.57 |
| MWS-Grt-1-02 | 9.36 | 2.79 | 5.50 | 0.60 | 2.63 | 0.47 | 1.13 | 0.16 | 1.06 | 0.18 | 1.89 | 0.62 | 9.11 |
| MWS-Grt-1-03 | 10.11 | 2.49 | 8.62 | 0.97 | 4.38 | 0.67 | 1.52 | 0.15 | 1.11 | 0.16 | 1.04 | 0.41 | 5.02 |
| MWS-Grt-1-04 | 9.65 | 1.86 | 13.7 | 2.10 | 11.1 | 1.91 | 4.78 | 0.74 | 4.63 | 0.83 | BDL | BDL | 3.56 |
| MWS-Grt-1-05 | 2.46 | 0.76 | 1.78 | 0.22 | 1.28 | 0.24 | 0.70 | 0.10 | 0.58 | 0.14 | 3.21 | 0.15 | 4.50 |
| MWS-Grt-1-06 | 2.33 | 0.78 | 1.75 | 0.21 | 1.19 | 0.21 | 0.71 | 0.10 | 0.68 | 0.09 | BDL | 0.10 | 2.35 |
| MWS-Grt-1-07 | 3.01 | 0.80 | 1.64 | 0.21 | 0.95 | 0.18 | 0.54 | 0.09 | 0.54 | 0.09 | 1.18 | 0.27 | 3.17 |
| MWS-Grt-1-08 | 3.7 | 1.12 | 2.06 | 0.27 | 1.36 | 0.20 | 0.55 | 0.09 | 0.47 | 0.09 | 0.38 | 0.15 | 2.03 |
| MWS-Grt-1-09 | 3.11 | 0.88 | 1.52 | 0.18 | 1.38 | 0.31 | 0.68 | 0.06 | 0.57 | 0.10 | 1.40 | 0.20 | 2.35 |
| MWS-Grt-1-10 | 2.21 | 0.68 | 1.96 | 0.24 | 1.24 | 0.22 | 0.87 | 0.09 | 0.70 | 0.13 | 19.1 | 0.90 | 13.2 |
| MWS-Grt-1-11 | 2.28 | 0.52 | 2.10 | 0.27 | 1.20 | 0.20 | 0.52 | 0.06 | 0.57 | 0.06 | 1.35 | 0.34 | 2.45 |
| MWS-Grt-1-12 | 4.82 | 1.02 | 3.13 | 0.32 | 2.20 | 0.47 | 1.26 | 0.21 | 1.45 | 0.22 | 50.1 | 2.08 | 16.4 |
| MWS-Grt-1-13 | 3.67 | 0.80 | 2.04 | 0.19 | 0.90 | 0.16 | 0.51 | 0.09 | 0.33 | 0.07 | 95.4 | 2.79 | 22.6 |
| MWS-Grt-1-14 | 4.05 | 1.23 | 2.81 | 0.38 | 2.15 | 0.29 | 1.08 | 0.11 | 1.60 | 0.21 | 0.84 | 0.20 | 2.58 |
| MWS-Grt-1-15 | 3.32 | 0.96 | 2.68 | 0.32 | 1.62 | 0.39 | 1.14 | 0.11 | 0.98 | 0.15 | 0.96 | 1.35 | 3.16 |
| MWS-Grt-1-16 | 2.63 | 0.85 | 2.44 | 0.24 | 1.50 | 0.25 | 0.79 | 0.14 | 0.57 | 0.15 | BDL | 0.20 | 2.19 |
| MWS-Grt-1-17 | 2.62 | 0.79 | 2.40 | 0.23 | 1.61 | 0.34 | 1.10 | 0.10 | 0.99 | 0.12 | BDL | 0.28 | 2.26 |
| MWS-Grt-1-18 | 2.82 | 0.83 | 2.36 | 0.21 | 1.64 | 0.22 | 0.70 | 0.11 | 1.13 | 0.15 | 0.55 | 0.17 | 1.98 |
| MWS-Grt-1-19 | 7.71 | 2.81 | 3.43 | 0.41 | 2.05 | 0.35 | 0.76 | 0.08 | 0.49 | 0.08 | 4.12 | 0.45 | 7.28 |
| MWS-Grt-1-20 | 6.75 | 2.32 | 4.18 | 0.40 | 1.93 | 0.38 | 1.09 | 0.13 | 1.02 | 0.14 | 1.61 | 0.44 | 7.37 |
| MWS-Grt-2-01 | BDL | 0.80 | 0.13 | BDL | 0.25 | BDL | BDL | BDL | BDL | BDL | 631 | BDL | 10.9 |
| MWS-Grt-2-02 | BDL | 0.79 | BDL | BDL | 0.08 | BDL | BDL | BDL | BDL | BDL | 556 | BDL | 7.95 |
| MWS-Grt-2-03 | BDL | 0.74 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 579 | 0.09 | 10.4 |
| MWS-Grt-2-04 | BDL | 1.06 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 538 | BDL | 11.2 |
| MWS-Grt-2-05 | BDL | 1.51 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 806 | BDL | 13.3 |
| MWS-Grt-2-06 | BDL | 1.24 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 531 | BDL | 15.8 |
| MWS-Grt-2-07 | BDL | 1.12 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 586 | BDL | 16.8 |
| MWS-Grt-2-08 | BDL | 1.20 | 0.58 | BDL | 0.55 | BDL | 0.28 | BDL | BDL | BDL | 568 | 0.13 | 11.4 |
| MWS-Grt-2-09 | BDL | 0.85 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 570 | BDL | 8.79 |
| MWS-Grt-2-10 | BDL | 0.73 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 388 | BDL | 14.9 |
| MWS-Grt-2-11 | BDL | 0.78 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 492 | BDL | 18.6 |
| MWS-Grt-2-12 | BDL | 0.66 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 538 | BDL | 11.9 |
| MWS-Grt-2-13 | BDL | 0.78 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 462 | BDL | 12.4 |
| MWS-Grt-2-14 | BDL | 0.44 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 504 | BDL | 8.70 |
| MWS-Grt-2-15 | BDL | 0.43 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 240 | BDL | 4.30 |
| MWS-Grt-2-16 | BDL | 0.37 | BDL | BDL | BDL | BDL | BDL | BDL | BDL | BDL | 514 | BDL | 5.47 |
| SRM 610 Reference values | 453 | 447 | 449 | 437 | 437 | 449 | 455 | 435 | 450 | 439 | 444 | 457 | 462 |
| SRM 610-1 | 517 | 492 | 506 | 486 | 492 | 507 | 516 | 478 | 519 | 479 | 476 | 503 | 489 |
| SRM 610-2 | 510 | 484 | 492 | 476 | 483 | 498 | 510 | 466 | 509 | 468 | 470 | 486 | 475 |
| SRM 610-3 | 490 | 466 | 473 | 460 | 467 | 476 | 491 | 443 | 482 | 450 | 451 | 474 | 465 |
| SRM 610-4 | 489 | 465 | 477 | 457 | 466 | 479 | 499 | 453 | 488 | 455 | 453 | 473 | 467 |
| SRM 610-5 | 486 | 465 | 475 | 459 | 466 | 477 | 488 | 451 | 483 | 452 | 448 | 470 | 464 |
| SRM 610-6 | 497 | 467 | 473 | 459 | 471 | 478 | 499 | 450 | 489 | 452 | 445 | 466 | 459 |
| SRM 612 Reference values | 37.7 | 35.6 | 37.3 | 37.6 | 35.5 | 38.3 | 38.0 | 36.8 | 39.2 | 37.0 | 38.0 | 37.8 | 37.4 |
| SRM 612-1 | 41.4 | 38.0 | 39.9 | 38.7 | 37.3 | 39.7 | 41.5 | 39.5 | 41.4 | 36.7 | 42.1 | 40.3 | 40.9 |
| SRM 612-2 | 38.0 | 37.8 | 36.8 | 38.6 | 34.7 | 39.1 | 39.4 | 36.9 | 39.9 | 37.0 | 39.9 | 37.7 | 39.2 |
| SRM 612-3 | 38.1 | 37.2 | 36.9 | 38.1 | 34.3 | 38.9 | 39.4 | 37.2 | 36.1 | 37.3 | 39.1 | 39.2 | 39.8 |
| SRM 612-4 | 36.2 | 35.5 | 35.6 | 37.0 | 38.5 | 38.9 | 38.7 | 35.9 | 39.5 | 35.8 | 37.0 | 37.5 | 39.2 |
| SRM 612-5 | 37.9 | 34.3 | 36.8 | 36.1 | 36.4 | 37.3 | 38.2 | 35.5 | 40.8 | 36.8 | 36.1 | 37.2 | 38.4 |
| SRM 612-6 | 35.9 | 34.2 | 34.0 | 36.2 | 35.1 | 37.3 | 38.5 | 35.3 | 36.6 | 36.0 | 37.7 | 37.1 | 37.4 |
| BCR-2G Reference values | 6.59 | 1.97 | 6.71 | 1.02 | 6.44 | 1.27 | 3.70 | 0.51 | 3.39 | 0.50 | 0.50 | 5.90 | 1.69 |
| BCR-2G-1 | 4.83 | 1.33 | 4.89 | 0.88 | 5.93 | 0.97 | 2.59 | 0.39 | 2.49 | 0.41 | 0.33 | 5.27 | 1.66 |
| BCR-2G-2 | 5.09 | 1.86 | 5.05 | 0.86 | 5.05 | 1.07 | 2.41 | 0.43 | 2.46 | 0.40 | 0.60 | 4.85 | 1.75 |
| BCR-2G-3 | 5.84 | 1.45 | 4.79 | 0.85 | 4.60 | 0.82 | 2.50 | 0.40 | 2.47 | 0.31 | 0.66 | 5.35 | 1.34 |
| BCR-2G-4 | 4.56 | 1.61 | 5.61 | 0.77 | 4.84 | 0.88 | 2.86 | 0.39 | 2.77 | 0.43 | 1.00 | 4.93 | 1.40 |
| BCR-2G-5 | 5.44 | 1.52 | 5.35 | 0.78 | 4.66 | 0.97 | 2.80 | 0.39 | 2.37 | 0.43 | 0.53 | 4.86 | 1.41 |
| BCR-2G-6 | 5.03 | 1.55 | 5.15 | 0.70 | 4.81 | 0.84 | 3.05 | 0.42 | 2.59 | 0.40 | 0.65 | 4.50 | 1.68 |

Table S4. The results of in-situ garnet U–Pb LA–ICP–MS dating of samples from the Maweishan deposit.

| Spot number | Pb206 | Pb207 | Pb208 | Th232 | U238 | Pb207/Pb206 ratio | Pb207/Pb206 2 sigma | Pb207/U235 ratio | Pb207/U235 2 sigma | Pb206/U238 ratio | Pb206/U238 2 sigma | rho |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MWS-01 | 0.1500 | 0.0194 | 0.0353 | 0.54 | 5.25 | 0.1312 | 0.0146 | 0.4337 | 0.0500 | 0.0238 | 0.0010 | 0.26 |
| MWS-02 | 0.1750 | 0.0217 | 0.0452 | 0.54 | 6.20 | 0.1256 | 0.0122 | 0.4121 | 0.0360 | 0.0239 | 0.0010 | 0.02 |
| MWS-03 | 0.0790 | 0.0101 | 0.0194 | 0.14 | 2.84 | 0.1234 | 0.0220 | 0.4254 | 0.0960 | 0.0239 | 0.0012 | 0.99 |
| MWS-04 | 0.2450 | 0.1480 | 0.3480 | 0.29 | 3.19 | 0.5855 | 0.0280 | 5.5230 | 0.5200 | 0.0673 | 0.0046 | 0.86 |
| MWS-05 | 0.1600 | 0.0398 | 0.0807 | 0.60 | 4.89 | 0.2476 | 0.0178 | 0.9881 | 0.0660 | 0.0290 | 0.0012 | 0.17 |
| MWS-06 | 0.3330 | 0.0592 | 0.1290 | 2.01 | 11.80 | 0.1722 | 0.0142 | 0.6180 | 0.0660 | 0.0254 | 0.0012 | 0.68 |
| MWS-07 | 0.1360 | 0.0277 | 0.0546 | 0.52 | 4.69 | 0.1916 | 0.0220 | 0.7287 | 0.1280 | 0.0262 | 0.0016 | 0.98 |
| MWS-08 | 0.5980 | 0.0377 | 0.0620 | 5.53 | 25.90 | 0.0610 | 0.0036 | 0.1803 | 0.0110 | 0.0213 | 0.0007 | 0.31 |
| MWS-09 | 0.2250 | 0.0304 | 0.0503 | 0.46 | 8.98 | 0.1320 | 0.0106 | 0.4249 | 0.0420 | 0.0232 | 0.0011 | 0.59 |
| MWS-10 | 0.5670 | 0.0322 | 0.0563 | 5.70 | 28.80 | 0.0560 | 0.0060 | 0.1541 | 0.0160 | 0.0201 | 0.0007 | 0.10 |
| MWS-11 | 0.1700 | 0.0148 | 0.0207 | 0.52 | 8.44 | 0.0842 | 0.0096 | 0.2395 | 0.0300 | 0.0206 | 0.0009 | 0.37 |
| MWS-12 | 0.0972 | 0.0093 | 0.0141 | 0.34 | 4.68 | 0.0938 | 0.0134 | 0.2766 | 0.0400 | 0.0213 | 0.0009 | 0.16 |
| MWS-13 | 0.2380 | 0.0278 | 0.0470 | 0.84 | 11.50 | 0.1157 | 0.0094 | 0.3377 | 0.0300 | 0.0211 | 0.0009 | 0.44 |
| MWS-14 | 0.1090 | 0.0104 | 0.0123 | 0.37 | 5.41 | 0.0943 | 0.0118 | 0.2671 | 0.0320 | 0.0208 | 0.0008 | 0.12 |
| MWS-15 | 0.1230 | 0.0195 | 0.0343 | 0.47 | 5.35 | 0.1498 | 0.0200 | 0.5015 | 0.0780 | 0.0239 | 0.0010 | 0.52 |
| MWS-16 | 0.2750 | 0.0320 | 0.0671 | 2.44 | 13.30 | 0.1136 | 0.0146 | 0.3401 | 0.0540 | 0.0214 | 0.0009 | 0.75 |
| MWS-17 | 0.4430 | 0.0445 | 0.0879 | 4.73 | 21.10 | 0.0979 | 0.0104 | 0.3023 | 0.0420 | 0.0219 | 0.0008 | 0.84 |
| MWS-18 | 0.1830 | 0.0176 | 0.0356 | 1.78 | 8.67 | 0.0929 | 0.0118 | 0.2851 | 0.0420 | 0.0221 | 0.0010 | 0.49 |
| MWS-19 | 0.1360 | 0.0169 | 0.0273 | 0.79 | 6.23 | 0.1208 | 0.0158 | 0.3853 | 0.0540 | 0.0230 | 0.0010 | 0.35 |
| MWS-20 | 0.2900 | 0.1600 | 0.3880 | 1.00 | 5.14 | 0.5468 | 0.0280 | 4.5050 | 0.4400 | 0.0590 | 0.0044 | 0.87 |
| MWS-21 | 0.2400 | 0.0239 | 0.0450 | 2.20 | 11.20 | 0.0980 | 0.0108 | 0.3074 | 0.0340 | 0.0227 | 0.0009 | 0.16 |
| MWS-22 | 0.2110 | 0.0249 | 0.0368 | 0.40 | 9.53 | 0.1139 | 0.0158 | 0.3750 | 0.0580 | 0.0231 | 0.0011 | 0.48 |
| MWS-23 | 0.2160 | 0.0355 | 0.0622 | 0.54 | 9.37 | 0.1576 | 0.0144 | 0.5321 | 0.0600 | 0.0240 | 0.0009 | 0.63 |
| MWS-24 | 0.2000 | 0.0250 | 0.0529 | 2.70 | 8.77 | 0.1211 | 0.0156 | 0.4076 | 0.0640 | 0.0238 | 0.0011 | 0.71 |
| MWS-25 | 0.1650 | 0.0336 | 0.0727 | 0.44 | 6.59 | 0.1919 | 0.0240 | 0.7302 | 0.1120 | 0.0262 | 0.0014 | 0.61 |
| MWS-26 | 0.2250 | 0.0202 | 0.0347 | 1.94 | 10.90 | 0.0878 | 0.0124 | 0.2647 | 0.0420 | 0.0217 | 0.0008 | 0.59 |
| MWS-27 | 0.1960 | 0.0136 | 0.0124 | 0.14 | 9.54 | 0.0683 | 0.0058 | 0.2010 | 0.0180 | 0.0212 | 0.0008 | 0.32 |
| MWS-28 | 0.2560 | 0.0248 | 0.0354 | 0.36 | 12.10 | 0.0966 | 0.0074 | 0.2906 | 0.0220 | 0.0219 | 0.0008 | 0.21 |
| MWS-29 | 0.2510 | 0.0622 | 0.1380 | 1.25 | 9.78 | 0.2373 | 0.0178 | 0.8910 | 0.0760 | 0.0271 | 0.0016 | 0.51 |
| MWS-30 | 0.1820 | 0.0349 | 0.0707 | 0.99 | 7.35 | 0.1840 | 0.0194 | 0.6700 | 0.0900 | 0.0254 | 0.0010 | 0.81 |
| MWS-31 | 0.2080 | 0.0158 | 0.0246 | 1.73 | 9.92 | 0.0735 | 0.0084 | 0.2153 | 0.0260 | 0.0212 | 0.0007 | 0.20 |
| MWS-32 | 0.1280 | 0.0133 | 0.0188 | 0.44 | 5.88 | 0.1001 | 0.0126 | 0.3131 | 0.0500 | 0.0223 | 0.0010 | 0.76 |
| MWS-33 | 0.0672 | 0.0066 | 0.0107 | 0.18 | 3.21 | 0.0948 | 0.0146 | 0.2784 | 0.0460 | 0.0215 | 0.0010 | 0.30 |
| MWS-34 | 0.0487 | 0.0088 | 0.0140 | 0.10 | 1.93 | 0.1689 | 0.0220 | 0.6062 | 0.0980 | 0.0257 | 0.0015 | 0.69 |
| MWS-35 | 0.1070 | 0.0144 | 0.0257 | 0.30 | 4.81 | 0.1293 | 0.0142 | 0.4058 | 0.0440 | 0.0228 | 0.0010 | 0.21 |
| MWS-36 | 0.2310 | 0.0210 | 0.0383 | 1.84 | 11.10 | 0.0856 | 0.0098 | 0.2515 | 0.0280 | 0.0215 | 0.0008 | 0.04 |
| MWS-37 | 0.1740 | 0.0382 | 0.0819 | 0.83 | 6.47 | 0.2086 | 0.0182 | 0.7964 | 0.0780 | 0.0276 | 0.0013 | 0.46 |
| Reference materials |  |  |  |  |  |  |  |  |  |  |  |  |
| MALI-01 | 0.6590 | 0.0337 | 0.0272 | 1.62 | 16.3 | 0.0512 | 0.0022 | 0.2281 | 0.0108 | 0.0321 | 0.0006 | 0.49 |
| MALI-02 | 0.6970 | 0.0573 | 0.0903 | 1.81 | 16.6 | 0.0829 | 0.0036 | 0.3824 | 0.0170 | 0.0334 | 0.0007 | 0.28 |
| MALI-03 | 0.6380 | 0.0396 | 0.0434 | 2.03 | 18.3 | 0.0623 | 0.0030 | 0.2774 | 0.0130 | 0.0324 | 0.0009 | 0.24 |
| MALI-04 | 0.6680 | 0.0353 | 0.0317 | 2.00 | 19.9 | 0.0529 | 0.0022 | 0.2289 | 0.0096 | 0.0314 | 0.0008 | 0.26 |
| MALI-05 | 0.5670 | 0.0288 | 0.0265 | 2.02 | 18.6 | 0.0509 | 0.0024 | 0.2246 | 0.0112 | 0.0320 | 0.0008 | 0.41 |
| MALI-06 | 0.6140 | 0.0350 | 0.0336 | 2.21 | 20.6 | 0.0573 | 0.0028 | 0.2489 | 0.0120 | 0.0315 | 0.0007 | 0.23 |
| MALI-07 | 0.5740 | 0.0315 | 0.0267 | 1.94 | 18.3 | 0.0549 | 0.0028 | 0.2468 | 0.0126 | 0.0325 | 0.0007 | 0.29 |
| MALI-08 | 0.5780 | 0.0300 | 0.0256 | 2.01 | 18.8 | 0.0521 | 0.0028 | 0.2278 | 0.0112 | 0.0318 | 0.0007 | 0.08 |
| MALI-09 | 0.4870 | 0.0276 | 0.0219 | 1.77 | 15.5 | 0.0561 | 0.0028 | 0.2480 | 0.0130 | 0.0321 | 0.0006 | 0.25 |
| MALI-10 | 0.5280 | 0.0302 | 0.0270 | 1.86 | 17.0 | 0.0568 | 0.0032 | 0.2487 | 0.0140 | 0.0318 | 0.0007 | 0.25 |
| ZSLS-01 | 0.8260 | 0.0480 | 0.7330 | 63.7 | 26.8 | 0.0583 | 0.0032 | 0.1990 | 0.0106 | 0.0248 | 0.0006 | 0.13 |
| ZSLS-02 | 0.6820 | 0.0351 | 0.5850 | 65.8 | 26.5 | 0.0518 | 0.0022 | 0.1732 | 0.0074 | 0.0242 | 0.0006 | 0.36 |
| ZSLS-03 | 0.6490 | 0.0333 | 0.5020 | 67.8 | 28.6 | 0.0515 | 0.0022 | 0.1716 | 0.0080 | 0.0241 | 0.0005 | 0.34 |
| ZSLS-04 | 0.6870 | 0.0355 | 0.5220 | 67.5 | 29.2 | 0.0516 | 0.0024 | 0.1742 | 0.0076 | 0.0244 | 0.0004 | 0.00 |
| ZSLS-05 | 0.5750 | 0.0308 | 0.5150 | 66.5 | 23.6 | 0.0530 | 0.0024 | 0.1812 | 0.0092 | 0.0248 | 0.0005 | 0.38 |
| Willsboro-01 | 0.2050 | 0.0190 | 0.0314 | 0.29 | 0.96 | 0.0932 | 0.0056 | 2.2220 | 0.1340 | 0.1735 | 0.0050 | 0.24 |
| Willsboro-02 | 0.1550 | 0.0132 | 0.0215 | 0.31 | 0.93 | 0.0875 | 0.0082 | 2.1020 | 0.1740 | 0.1782 | 0.0062 | 0.17 |
| Willsboro-03 | 0.1450 | 0.0131 | 0.0217 | 0.28 | 0.87 | 0.0911 | 0.0068 | 2.1540 | 0.1520 | 0.1732 | 0.0048 | 0.02 |
| Willsboro-04 | 0.1440 | 0.0149 | 0.0248 | 0.28 | 0.83 | 0.1031 | 0.0096 | 2.5190 | 0.2400 | 0.1778 | 0.0054 | 0.23 |

Table S5. LA–ICP–MS data for sphalerite from the Maweishan deposit analyzed during this study (in ppm, BDL = Below the Detection Limit).

| Spot number | Mn | Fe | Cu | Zn | Ga | Ge | As | Ag | Cd | In | Sn | Sb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Detection limit | 1.31 | 5.86 | 0.38 | 4.26 | 0.26 | 2.02 | 1.41 | 0.25 | 1.69 | 0.07 | 0.27 | 0.23 |
| MWS-SP1-01 | 4256 | 71582 | 409 | 575240 | 71.0 | BDL | BDL | 9.31 | 4727 | 175 | 14.6 | 0.80 |
| MWS-SP1-02 | 4164 | 71595 | 193 | 575908 | 61.0 | BDL | 2.08 | 8.15 | 4606 | 179 | 18.4 | 0.25 |
| MWS-SP1-03 | 4167 | 71511 | 135 | 576156 | 22.4 | BDL | 2.38 | 7.14 | 4635 | 171 | 18.3 | 0.05 |
| MWS-SP1-04 | 3639 | 69049 | 941 | 577246 | 75.3 | BDL | 2.67 | 13.0 | 4630 | 176 | 6.56 | 3.60 |
| MWS-SP1-05 | 4042 | 72170 | 206 | 575481 | 96.0 | BDL | BDL | 9.44 | 4172 | 169 | 11.4 | 0.54 |
| MWS-SP1-06 | 4069 | 72021 | 194 | 575301 | 89.4 | BDL | 1.66 | 9.29 | 4563 | 175 | 18.0 | 0.05 |
| MWS-SP1-07 | 4129 | 73139 | 587 | 573133 | 124 | BDL | 2.36 | 11.1 | 5107 | 132 | 16.5 | 0.40 |
| MWS-SP1-08 | 4122 | 72924 | 255 | 573868 | 164 | BDL | 2.16 | 11.3 | 4969 | 143 | 17.9 | 0.04 |
| MWS-SP1-09 | 4080 | 73399 | 120 | 573919 | 67.3 | BDL | 1.87 | 6.11 | 4865 | 78.3 | 14.3 | 0.01 |
| MWS-SP1-10 | 4017 | 70051 | 482 | 577207 | 141 | BDL | BDL | 23.9 | 4735 | 173 | 20.9 | 2.31 |
| MWS-SP1-11 | 3942 | 70650 | 476 | 576628 | 76.2 | BDL | 5.18 | 21.1 | 4786 | 175 | 9.36 | 3.02 |
| MWS-SP1-12 | 3990 | 72012 | 206 | 575557 | 83.0 | BDL | 1.72 | 8.14 | 4680 | 174 | 14.4 | 0.15 |
| MWS-SP2-01 | 2246 | 71220 | 192 | 576981 | 206 | BDL | 21.5 | 142 | 3723 | 103 | 7.85 | 14.3 |
| MWS-SP2-02 | 2653 | 61203 | 193 | 590979 | 198 | BDL | 1.90 | 139 | 3642 | 101 | 6.12 | 4.37 |
| MWS-SP2-03 | 2749 | 58362 | 181 | 594091 | 170 | BDL | 10.4 | 107 | 3704 | 114 | 7.82 | 8.98 |
| MWS-SP2-04 | 2993 | 62082 | 178 | 589125 | 152 | BDL | 1.48 | 91.0 | 4190 | 121 | 7.79 | 0.13 |
| MWS-SP2-05 | 3746 | 61683 | 247 | 587918 | 230 | BDL | 1.58 | 147 | 3772 | 142 | 9.52 | 8.38 |
| MWS-SP2-06 | 5169 | 64654 | 222 | 582573 | 207 | BDL | 1.59 | 116 | 3930 | 125 | 3.40 | 0.01 |
| MWS-SP2-07 | 3654 | 63395 | 208 | 586747 | 175 | BDL | 2.00 | 81.6 | 3849 | 138 | 9.25 | 6.01 |
| MWS-SP2-08 | 3462 | 63180 | 169 | 587402 | 152 | BDL | BDL | 104 | 3744 | 129 | 5.61 | 2.52 |
| MWS-SP2-09 | 4396 | 45556 | 171 | 605609 | 173 | BDL | 2.65 | 138 | 4105 | 119 | 11.6 | 9.97 |
| MWS-SP2-10 | 3437 | 44774 | 127 | 607914 | 103 | BDL | 38.7 | 131 | 4108 | 124 | 6.19 | 1.41 |
| MWS-SP2-11 | 2784 | 45375 | 150 | 608448 | 116 | BDL | 3.03 | 67.5 | 4211 | 122 | 6.93 | BDL |
| MWS-SP2-12 | 2629 | 45339 | 182 | 608692 | 185 | BDL | 2.92 | 151 | 4187 | 109 | 8.75 | 3.33 |
| MWS-SP2-13 | 2465 | 55449 | 194 | 595536 | 204 | BDL | 81.7 | 187 | 3927 | 109 | 7.14 | 19.4 |
| MWS-SP2-14 | 5191 | 45831 | 137 | 604047 | 110 | BDL | 2.55 | 85.4 | 4084 | 120 | 5.62 | BDL |
| MWS-SP3-01 | 3882 | 32966 | 291 | 620977 | 202 | BDL | 3.05 | 48.5 | 3953 | 187 | 3.61 | BDL |
| MWS-SP3-02 | 4043 | 34214 | 429 | 618570 | 111 | BDL | 3.56 | 44.8 | 4016 | 178 | 27.8 | 3.32 |
| MWS-SP3-03 | 3406 | 32461 | 770 | 621470 | 245 | BDL | 4.03 | 44.8 | 3855 | 168 | 9.62 | 5.22 |
| MWS-SP3-04 | 3215 | 35951 | 211 | 618697 | 106 | BDL | 2.93 | 50.0 | 4159 | 168 | 22.2 | 11.7 |
| MWS-SP3-05 | 2981 | 36189 | 214 | 618553 | 133 | BDL | 8.03 | 30.9 | 4269 | 162 | 12.1 | 0.29 |
| MWS-SP3-06 | 3199 | 35337 | 281 | 619534 | 168 | BDL | 3.50 | 43.0 | 4101 | 161 | 8.75 | 2.08 |
| MWS-SP3-07 | 3677 | 36170 | 1062 | 616629 | 172 | BDL | 3.69 | 65.3 | 4131 | 170 | 9.18 | 7.48 |
| MWS-SP3-08 | 3626 | 35004 | 280 | 614223 | 212 | BDL | 7.65 | 65.6 | 4075 | 163 | 8.28 | 14.0 |
| MWS-SP3-09 | 3224 | 34966 | 191 | 619662 | 109 | BDL | 3.51 | 73.9 | 4129 | 155 | 8.48 | 1.46 |
| MWS-SP3-10 | 3542 | 32845 | 272 | 621437 | 201 | BDL | 3.39 | 62.9 | 3923 | 170 | 15.7 | 2.38 |
| MWS-SP3-11 | 3534 | 34276 | 275 | 620204 | 176 | BDL | 6.52 | 58.2 | 4049 | 170 | 1.80 | 5.92 |
| MWS-SP3-12 | 2959 | 33273 | 266 | 621971 | 182 | BDL | 2.57 | 60.5 | 4019 | 162 | 3.81 | 0.49 |
| MWS-SP3-13 | 2924 | 39544 | 162 | 615707 | 81.6 | BDL | BDL | 42.5 | 3937 | 158 | 5.84 | 0.35 |
| MWS-SP3-14 | 3102 | 39337 | 186 | 615583 | 102 | BDL | 1.73 | 43.9 | 3905 | 158 | 7.21 | 0.96 |
| MWS-SP3-15 | 3381 | 38124 | 293 | 616195 | 221 | BDL | 1.98 | 55.3 | 3917 | 174 | 10.2 | 0.83 |
| MWS-SP3-16 | 2704 | 36217 | 362 | 619402 | 204 | BDL | 15.3 | 76.7 | 3864 | 166 | 32.5 | 17.4 |
| MWS-SP3-17 | 3258 | 40792 | 184 | 613684 | 93.6 | BDL | 1.99 | 30.4 | 3836 | 178 | 5.29 | 1.02 |
| MWS-SP3-18 | 3201 | 42111 | 195 | 611739 | 105 | BDL | 1.42 | 35.0 | 4333 | 176 | 6.48 | 2.48 |
| MWS-SP3-19 | 2917 | 38801 | 538 | 615306 | 55.3 | BDL | 1.26 | 47.0 | 4256 | 170 | 8.69 | 3.93 |
| MWS-SP3-20 | 5845 | 39073 | 295 | 608009 | 116 | BDL | 428 | 51.1 | 3529 | 146 | 9.11 | 9.99 |
| MWS-SP3-21 | 2421 | 40299 | 248 | 615541 | 104 | BDL | 3.42 | 105 | 3480 | 315 | 6.89 | 18.3 |
| MWS-SP3-22 | 3281 | 44733 | 208 | 609481 | 54.6 | BDL | 1.73 | 33.9 | 3582 | 274 | 3.45 | 0.73 |
| MWS-SP3-23 | 3353 | 45209 | 244 | 608659 | 70.6 | BDL | 1.28 | 35.4 | 3662 | 322 | 2.38 | BDL |
| MWS-SP3-24 | 3111 | 43619 | 310 | 610718 | 250 | BDL | 6.00 | 70.7 | 3709 | 146 | 1.33 | 1.49 |
| MWS-SP3-25 | 2893 | 42739 | 322 | 611065 | 234 | BDL | 17.5 | 119 | 3638 | 156 | 56.7 | 33.9 |
| MWS-SP3-26 | 3592 | 41942 | 292 | 611580 | 68.5 | BDL | BDL | 68.4 | 3683 | 407 | 4.82 | 3.08 |
| MWS-SP3-27 | 3454 | 41298 | 242 | 612260 | 80.7 | BDL | 2.29 | 108 | 3645 | 295 | 13.9 | 17.8 |
| MWS-SP3-28 | 3451 | 41248 | 332 | 612580 | 233 | BDL | 0.59 | 112 | 3701 | 214 | 1.11 | 13.6 |
| MWS-SP3-29 | 3340 | 40483 | 406 | 613370 | 348 | BDL | 2.31 | 71.4 | 3717 | 162 | 2.23 | BDL |
| SRM 610 Reference values | 444 | 458 | 441 | 460 | 433 | 447 | 325 | 251 | 270 | 434 | 430 | 396 |
| SRM 610-1 | 442 | 452 | 454 | 472 | 439 | 421 | 347 | 272 | 282 | 459 | 441 | 394 |
| SRM 610-2 | 450 | 471 | 450 | 480 | 447 | 448 | 348 | 268 | 294 | 472 | 465 | 410 |
| SRM 610-3 | 442 | 439 | 424 | 474 | 428 | 415 | 316 | 234 | 258 | 422 | 408 | 396 |
| SRM 610-4 | 445 | 458 | 438 | 464 | 441 | 418 | 323 | 250 | 274 | 433 | 432 | 422 |
| SRM 610-5 | 459 | 444 | 448 | 481 | 446 | 433 | 334 | 241 | 258 | 439 | 427 | 406 |
| SRM 610-6 | 455 | 462 | 447 | 478 | 437 | 434 | 338 | 244 | 265 | 440 | 423 | 403 |
| SRM 610-7 | 438 | 456 | 431 | 482 | 431 | 414 | 334 | 245 | 270 | 430 | 418 | 393 |
| SRM 612 Reference values | 38.7 | 51.0 | 37.8 | 39.1 | 36.9 | 36.1 | 35.7 | 22.0 | 28.1 | 38.9 | 38.6 | 34.7 |
| SRM 612-1 | 37.3 | 87.0 | 38.1 | 33.4 | 35.7 | 34.7 | 36.7 | 22.4 | 27.5 | 36.7 | 36.9 | 32.4 |
| SRM 612-2 | 39.3 | 90.8 | 38.0 | 37.4 | 37.2 | 35.7 | 34.6 | 20.7 | 26.8 | 37.0 | 36.8 | 35.2 |
| SRM 612-3 | 38.4 | 75.8 | 36.6 | 38.4 | 35.8 | 35.0 | 35.1 | 20.7 | 25.8 | 35.7 | 36.5 | 32.6 |
| SRM 612-4 | 37.7 | 69.0 | 37.6 | 35.6 | 35.4 | 35.5 | 35.4 | 21.0 | 25.3 | 36.3 | 36.9 | 32.9 |
| SRM 612-5 | 36.5 | 72.0 | 36.9 | 36.1 | 35.5 | 34.7 | 35.8 | 20.8 | 22.9 | 35.8 | 35.8 | 32.3 |
| SRM 612-6 | 38.3 | 48.4 | 38.6 | 39.5 | 37.3 | 35.7 | 44.2 | 23.4 | 30.0 | 39.9 | 40.5 | 35.0 |
| SRM 612-7 | 37.2 | 63.1 | 35.9 | 36.5 | 34.6 | 35.1 | 36.4 | 20.1 | 24.5 | 34.3 | 34.4 | 32.4 |
| BCR-2G Reference values | 1550 | 96387 | 21.0 | 125 | 23.0 | 1.50 | - | 0.50 | 0.20 | 0.11 | 2.60 | 0.35 |
| BCR-2G-1 | 1483 | 80261 | 17.6 | 148 | 21.6 | 2.0 | 3.1 | 0.58 | 0.22 | 0.09 | 2.23 | 0.32 |
| BCR-2G-2 | 1448 | 79555 | 16.5 | 163 | 21.4 | 1.9 | 4.2 | 0.59 | 0.09 | 0.11 | 2.10 | 0.29 |
| BCR-2G-3 | 1540 | 82394 | 16.3 | 164 | 20.5 | 1.5 | 4.6 | 0.49 | 0.84 | 0.09 | 2.32 | 0.39 |
| BCR-2G-4 | 1450 | 83141 | 16.1 | 167 | 21.0 | 1.6 | 3.9 | 0.58 | 0.92 | 0.10 | 2.53 | 0.33 |
| BCR-2G-5 | 1497 | 85437 | 17.0 | 159 | 21.8 | 2.4 | 4.7 | 0.59 | 0.13 | 0.11 | 1.79 | 0.35 |
| BCR-2G-6 | 1463 | 91459 | 17.5 | 154 | 22.5 | 1.7 | 6.3 | 0.48 | 0.21 | 0.10 | 2.63 | 0.36 |
| BCR-2G-7 | 1469 | 93145 | 18.0 | 156 | 21.6 | 1.2 | 7.1 | 0.54 | 0.27 | 0.10 | 2.14 | 0.42 |

Table S6. Sulfur isotopic data for samples from the Maweishan deposit.

| Spot number | Host mineral | δ34S | Spot number | Host mineral | δ34S |
| --- | --- | --- | --- | --- | --- |
| MWS-Ccp-01 | Chalcopyrite (Quartz-sulfide) | 7.47 | MWS-Py-06 | Pyrite (Calcite-sulfide) | 8.06 |
| MWS-Ccp-02 | Chalcopyrite (Quartz-sulfide) | 5.29 | MWS-Po-01 | Pyrrhotite (Quartz-sulfide) | 6.07 |
| MWS-Ccp-03 | Chalcopyrite (Quartz-sulfide) | 6.66 | MWS-Po-02 | pyrrhotite (Quartz-sulfide) | 6.10 |
| MWS-Ccp-04 | Chalcopyrite (Calcite-sulfide) | 7.48 | MWS-Po-03 | pyrrhotite (Quartz-sulfide) | 6.15 |
| MWS-Ccp-05 | Chalcopyrite (Calcite-sulfide) | 8.11 | MWS-Po-04 | pyrrhotite (Quartz-sulfide) | 5.83 |
| MWS-Py-01 | Pyrite (Quartz-sulfide) | 4.87 | MWS-Sp-01 | sphalerite (Quartz-sulfide) | 6.17 |
| MWS-Py-02 | Pyrite (Quartz-sulfide) | 4.93 | MWS-Sp-02 | sphalerite (Quartz-sulfide) | 5.25 |
| MWS-Py-03 | Pyrite (Quartz-sulfide) | 6.98 | MWS-Sp-03 | sphalerite (Calcite-sulfide) | 5.18 |
| MWS-Py-04 | Pyrite (Calcite-sulfide) | 8.34 | MWS-Sp-04 | sphalerite (Calcite-sulfide) | 6.19 |
| MWS-Py-05 | Pyrite (Calcite-sulfide) | 7.93 | MWS-Sp-05 | sphalerite (Calcite-sulfide) | 6.29 |
| Reference materials |  |  |  |  |  |
| WS-1 | +1.1 ± 0.2‰ (Reference value) |  | NBS-123 | +17.1 ± 0.2‰ (Reference value) |  |
| WS-1-01 | +0.9 |  | WS-1-02 | +1.2 |  |
| WS-1-03 | +1.0 |  | WS-1-04 | +1.1 |  |
| NBS123-01 | +17.2 |  | NBS123-02 | +17.0 |  |